Supplemental Materials

Ca(OH)2-Modified Camellia oleifera shell biochar: preparation, characterization and adsorption of NH4+ and PO43-

Min Chen †,1, Xichang Wu †,1, Yu Wang 1, Jie Wang 2*, Chaochan Li1, Tianhua Yu 1, Anping Wang 1*

1 Key Laboratory of Mountain Information System and Ecological Environment Protection, Guizhou Normal University, Guiyang, 550025, China.

2 Qiandongnan Agriculture Science Institute, Kai Li, 556099, China.

† Min Chen and Xichang Wu are co-first-authors and contributed equally to this paper.

* Corresponding author, E-mail: xbmdwjie@163.com (JW);

anping-wang@gznu.edu.cn (AW)

Table S1 Preparation of modified biochar for adsorption of NH4+ and PO43-

| Serial Number | Name | m （g） | Chemical reagents | Water （mL） | Pyrolysis temperature （℃） | Pyrolysis time （h） |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | BC1-500 | 20 | 20 g CaCl2·2H2O | 150 | 500 | 2 |
| 2 | BC1-600 | 20 | 20 g CaCl2·2H2O | 150 | 600 | 2 |
| 3 | BC2-500 | 10 | 10 g C2H4N4、30 g FeCl3·6H2O | 120 | 500 | 2 |
| 4 | BC2-600 | 10 | 10 g C2H4N4、30 g FeCl3·6H2O | 120 | 600 | 2 |
| 5 | BC3-500 | 10 | 0.02 mol FeCl3·6H2O、0.04 mol Mg(OH)2 | 100 | 500 | 2 |
| 6 | BC4-500 | 10 | 0.1 mol MgO | 100 | 500 | 2 |
| 7 | BC4-600 | 10 | 0.1 mol MgO | 100 | 600 | 2 |
| 8 | BC5-500 | 10 | 20 g Ca(OH)2 | 100 | 500 | 2 |
| 9 | BC5-600 | 10 | 20 g Ca(OH)2 | 100 | 600 | 2 |

Note: m represents the mass of the powdered Camellia oleifera shells.

Experimental Details

All batch adsorption experiments were performed in a constant-temperature shaker at 150 rpm, unless otherwise indicated. The detailed experimental design is outlined below:

Adsorption kinetics: A 0.05 g portion of BC5-500 was added to 30 mL of NH4+ solution (100 mgL-1, pH 10.0) or PO43- solution (600 mgL-1, pH 6.0). The mixture was shaken at 25°C, and samples were collected at predetermined time intervals between 10 and 420 min to determine the variation of adsorption capacity over time.

Adsorption isotherms: NH4+ solutions (20-200 mgL-1) and PO43- solutions (200-1200 mgL-1) were prepared and adjusted to pH 10.0 and pH 6.0, respectively. For each concentration, 30 mL of solution was mixed with 0.05 g of BC5-500 and shaken at 25°C until adsorption equilibrium was reached.

Effect of solution pH: The pH of NH4+ (100 mgL-1) and PO43- (600 mgL-1) solutions was adjusted across the range of 2.0-12.0. Then, 30 mL of each solution was combined with 0.05 g of BC5-500 and shaken at 25°C until equilibrium was attained.

Effect of temperature: Experiments were conducted at temperatures ranging from 20 to 45°C. In each test, 0.05 g of BC5-500 was added to 30 mL of NH4+ solution (100 mgL-1, pH 10.0) or PO43- solution (600 mgL-1, pH 6.0). After shaking for 120 min (for NH4+) or 360 min (for NH4+), samples were collected for analysis.

Characterization Instruments Used in the Experiments

The characterization analyses of the samples were performed using a suite of analytical instruments, including a scanning electron microscope (Apreo 2, Thermo Fisher Scientific, USA), a specific surface area analyzer (TriStar II Plus, Micromeritics, USA), a Fourier-transform infrared spectrometer (Nicolet iS10, Thermo Scientific, USA), an X-ray photoelectron spectrometer (Escalab 250Xi, Thermo Fisher Scientific, USA), and an X-ray diffractometer (SmartLab 9 kW, Rigaku, Japan).