Tailoring porosity and surface chemistry of Sargassum biochar for enhanced CO2 capture

YuanlingLia,b, Tao Wangb, c, Jinyu Zhua, Siyu Duana, Lina Liub, *

aSchool of Environment and Resources, Taiyuan University of Science and Technology, Taiyuan, Shanxi 030024, China

bCollege of Environmental Science and Engineering, Nankai University, Tianjin 300350, China

cSchool of Environment and Energy, Peking University, Shenzhen Graduate School, Shenzhen 518055, China

* Corresponding Authors. Emails: liuln@nankai.edu.cn (L. Liu)

Text 1

Adsorptive kinetics models

The adsorption kinetics could be described by the pseudo-first order model:

qt=qe(1-e-k1t)

pseudo-second order model:

qt=t∙k2∙qe21+qe∙t∙k2

Where, qt (mg/g) and qe (mg/g) are the adsorption amount of CO2 at time t (min) and equilibrium, respectively; k1(1 min−1)and k2 (g/(mg min)) are adsorption rate constants.

Table S1 The isotherm data of N2 adsorption-desorption isotherms

| Relative pressure | Quantity adsorbed | Relative pressure | Quantity adsorbed | Relative pressure | Quantity adsorbed | Relative pressure | Quantity adsorbed | Relative pressure | Quantity adsorbed | Relative pressure | Quantity adsorbed |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P/Po | cm³/g STP | P/P0 | cm³/g STP | P/P0 | cm³/g STP | P/P0 | cm³/g STP | P/P0 | cm³/g STP | P/P0 | cm³/g STP |
|  | SBC400 |  | SBC400-KOH |  | Sar-KOH |  | SBC500 |  | SBC600 |  | SBC700 |
| 0.01 | 0.16 | 0.00 | 2.01 |  |  |  |  |  |  |  |  |
| 0.03 | 0.21 | 0.01 | 2.11 | 0.00 | 4.80 | 0.03 | 0.22 | 0.03 | 0.34 | 0.03 | 4.03 |
| 0.07 | 0.24 | 0.04 | −1.01 | 0.00 | 9.59 | 0.07 | 0.26 | 0.07 | 0.44 | 0.07 | 4.23 |
| 0.08 | 0.26 | 0.11 | −0.41 | 0.00 | 14.16 | 0.08 | 0.28 | 0.08 | 0.47 | 0.08 | 4.26 |
| 0.10 | 0.27 | 0.16 | −0.02 | 0.00 | 18.74 | 0.10 | 0.30 | 0.10 | 0.52 | 0.10 | 4.32 |
| 0.12 | 0.27 | 0.18 | 0.16 | 0.00 | 23.31 | 0.12 | 0.32 | 0.12 | 0.56 | 0.12 | 4.37 |
| 0.14 | 0.28 | 0.23 | 0.45 | 0.00 | 28.09 | 0.14 | 0.32 | 0.14 | 0.60 | 0.14 | 4.40 |
| 0.18 | 0.28 | 0.26 | 0.65 | 0.00 | 33.12 | 0.18 | 0.33 | 0.16 | 0.64 | 0.16 | 4.43 |
| 0.20 | 0.28 | 0.32 | 1.06 | 0.00 | 37.87 | 0.20 | 0.34 | 0.18 | 0.66 | 0.18 | 4.46 |
| 0.22 | 0.28 | 0.37 | 1.38 | 0.00 | 42.60 | 0.22 | 0.34 | 0.20 | 0.70 | 0.20 | 4.48 |
| 0.27 | 0.27 | 0.40 | 1.58 | 0.00 | 47.28 | 0.27 | 0.34 | 0.25 | 0.77 | 0.25 | 4.57 |
| 0.32 | 0.26 | 0.45 | 1.88 | 0.00 | 52.14 | 0.32 | 0.34 | 0.30 | 0.86 | 0.30 | 4.68 |
| 0.37 | 0.24 | 0.50 | 2.19 | 0.00 | 56.67 | 0.37 | 0.34 | 0.35 | 0.94 | 0.35 | 4.76 |
| 0.42 | 0.22 | 0.55 | 2.57 | 0.00 | 61.46 | 0.42 | 0.31 | 0.40 | 1.00 | 0.42 | 4.84 |
| 0.47 | 0.19 | 0.60 | 2.98 | 0.00 | 65.81 | 0.47 | 0.27 | 0.47 | 1.02 | 0.47 | 4.90 |
| 0.52 | 0.15 | 0.65 | 3.49 | 0.00 | 69.94 | 0.52 | 0.21 | 0.52 | 1.02 | 0.52 | 4.94 |
| 0.57 | 0.12 | 0.70 | 4.23 | 0.00 | 74.22 | 0.57 | 0.20 | 0.57 | 1.05 | 0.57 | 4.99 |
| 0.62 | 0.08 | 0.75 | 5.17 | 0.00 | 78.73 | 0.62 | 0.13 | 0.62 | 1.07 | 0.62 | 5.05 |
| 0.67 | 0.05 | 0.80 | 6.53 | 0.00 | 82.98 | 0.67 | 0.08 | 0.67 | 1.07 | 0.67 | 5.14 |
| 0.72 | 0.02 | 0.82 | 7.20 | 0.00 | 87.54 | 0.72 | 0.03 | 0.72 | 1.11 | 0.72 | 5.27 |
| 0.77 | 0.01 | 0.85 | 8.26 | 0.00 | 91.96 | 0.77 | −0.01 | 0.77 | 1.16 | 0.75 | 5.40 |
| 0.82 | 0.02 | 0.87 | 9.29 | 0.00 | 96.07 | 0.82 | −0.01 | 0.82 | 1.26 | 0.80 | 5.64 |
| 0.84 | 0.04 | 0.90 | 10.46 | 0.00 | 99.87 | 0.84 | 0.00 | 0.84 | 1.32 | 0.82 | 5.84 |
| 0.85 | 0.06 | 0.92 | 11.96 | 0.01 | 103.45 | 0.87 | 0.03 | 0.85 | 1.37 | 0.85 | 6.13 |
| 0.88 | 0.10 | 0.95 | 14.02 | 0.03 | 125.15 | 0.89 | 0.06 | 0.88 | 1.46 | 0.87 | 6.47 |
| 0.90 | 0.17 | 0.97 | 17.52 | 0.06 | 134.36 | 0.92 | 0.13 | 0.92 | 1.73 | 0.90 | 6.91 |
| 0.93 | 0.31 | 0.98 | 19.28 | 0.08 | 138.23 | 0.93 | 0.16 | 0.93 | 1.88 | 0.92 | 7.47 |
| 0.95 | 0.53 | 0.99 | 22.73 | 0.10 | 142.27 | 0.95 | 0.33 | 0.95 | 2.16 | 0.95 | 8.08 |
| 0.97 | 1.05 | 0.99 | 25.93 | 0.12 | 145.60 | 0.97 | 0.73 | 0.99 | 3.46 | 0.97 | 8.84 |
| 0.98 | 1.32 | 0.98 | 21.57 | 0.14 | 148.57 | 0.98 | 0.92 | 1.00 | 4.22 | 0.98 | 9.20 |
| 0.99 | 2.00 | 0.96 | 18.49 | 0.16 | 151.30 | 0.99 | 1.38 | 0.97 | 3.06 | 0.99 | 9.94 |
| 0.99 | 2.74 | 0.93 | 15.72 | 0.18 | 153.79 | 0.99 | 1.90 | 0.93 | 2.37 | 0.99 | 10.58 |
| 0.98 | 1.42 | 0.91 | 13.97 | 0.20 | 156.14 | 0.97 | 1.01 | 0.91 | 2.16 | 0.97 | 9.32 |
| 0.96 | 0.90 | 0.88 | 12.69 | 0.25 | 161.44 | 0.93 | 0.53 | 0.88 | 2.03 | 0.93 | 8.51 |
| 0.93 | 0.58 | 0.86 | 11.72 | 0.30 | 166.95 | 0.91 | 0.42 | 0.86 | 1.90 | 0.91 | 8.26 |
| 0.91 | 0.40 | 0.83 | 10.82 | 0.35 | 171.85 | 0.88 | 0.40 | 0.85 | 1.87 | 0.88 | 8.05 |
| 0.88 | 0.29 | 0.83 | 10.55 | 0.40 | 176.75 | 0.86 | 0.41 | 0.83 | 1.79 | 0.88 | 7.99 |
| 0.86 | 0.22 | 0.80 | 9.81 | 0.45 | 181.53 | 0.83 | 0.43 | 0.78 | 1.65 | 0.85 | 7.75 |
| 0.83 | 0.17 | 0.75 | 8.37 | 0.50 | 186.32 | 0.81 | 0.45 | 0.75 | 1.58 | 0.83 | 7.53 |
| 0.81 | 0.14 | 0.70 | 7.08 | 0.55 | 191.34 | 0.78 | 0.47 | 0.68 | 1.47 | 0.80 | 7.33 |
| 0.78 | 0.13 | 0.65 | 6.11 | 0.60 | 196.66 | 0.73 | 0.52 | 0.63 | 1.41 | 0.75 | 7.06 |
| 0.73 | 0.12 | 0.60 | 5.34 | 0.65 | 202.42 | 0.68 | 0.57 | 0.58 | 1.35 | 0.70 | 6.89 |
| 0.68 | 0.12 | 0.55 | 4.71 | 0.70 | 209.12 | 0.63 | 0.61 | 0.53 | 1.27 | 0.63 | 6.74 |
| 0.63 | 0.14 | 0.50 | 4.14 | 0.75 | 217.61 | 0.58 | 0.64 | 0.48 | 1.14 | 0.58 | 6.65 |
| 0.58 | 0.16 | 0.45 | 3.15 | 0.80 | 227.89 | 0.53 | 0.66 | 0.45 | 1.08 | 0.53 | 6.57 |
| 0.53 | 0.19 | 0.40 | 2.59 | 0.82 | 233.51 | 0.48 | 0.66 | 0.38 | 0.92 | 0.48 | 6.26 |
| 0.48 | 0.19 | 0.33 | 2.12 | 0.85 | 242.64 | 0.43 | 0.65 | 0.33 | 0.85 | 0.45 | 5.89 |
| 0.43 | 0.19 | 0.28 | 1.80 | 0.87 | 252.56 | 0.38 | 0.61 | 0.28 | 0.77 | 0.40 | 5.67 |
| 0.38 | 0.20 | 0.25 | 1.61 | 0.90 | 265.34 | 0.33 | 0.58 | 0.23 | 0.68 | 0.33 | 5.46 |
| 0.33 | 0.20 | 0.20 | 1.29 | 0.92 | 282.74 | 0.28 | 0.55 | 0.18 | 0.58 | 0.28 | 5.33 |
| 0.28 | 0.20 | 0.14 | 0.81 | 0.95 | 317.28 | 0.23 | 0.51 | 0.12 | 0.38 | 0.25 | 5.23 |
| 0.23 | 0.21 |  |  | 0.97 | 375.46 | 0.18 | 0.45 |  |  | 0.20 | 5.09 |
| 0.18 | 0.20 |  |  | 0.98 | 407.25 | 0.14 | 0.39 |  |  | 0.14 | 4.88 |
| 0.12 | 0.17 |  |  | 0.99 | 449.46 |  |  |  |  |  |  |
|  |  |  |  | 0.99 | 486.47 |  |  |  |  |  |  |
|  |  |  |  | 0.98 | 473.89 |  |  |  |  |  |  |
|  |  |  |  | 0.98 | 457.21 |  |  |  |  |  |  |
|  |  |  |  | 0.97 | 440.56 |  |  |  |  |  |  |
|  |  |  |  | 0.95 | 379.04 |  |  |  |  |  |  |
|  |  |  |  | 0.93 | 328.57 |  |  |  |  |  |  |
|  |  |  |  | 0.90 | 292.69 |  |  |  |  |  |  |
|  |  |  |  | 0.87 | 266.56 |  |  |  |  |  |  |
|  |  |  |  | 0.84 | 253.77 |  |  |  |  |  |  |
|  |  |  |  | 0.83 | 247.83 |  |  |  |  |  |  |
|  |  |  |  | 0.80 | 239.15 |  |  |  |  |  |  |
|  |  |  |  | 0.75 | 226.85 |  |  |  |  |  |  |
|  |  |  |  | 0.70 | 217.70 |  |  |  |  |  |  |
|  |  |  |  | 0.65 | 210.27 |  |  |  |  |  |  |
|  |  |  |  | 0.60 | 203.59 |  |  |  |  |  |  |
|  |  |  |  | 0.55 | 198.11 |  |  |  |  |  |  |
|  |  |  |  | 0.50 | 193.14 |  |  |  |  |  |  |
|  |  |  |  | 0.45 | 186.27 |  |  |  |  |  |  |
|  |  |  |  | 0.40 | 179.36 |  |  |  |  |  |  |
|  |  |  |  | 0.35 | 174.30 |  |  |  |  |  |  |
|  |  |  |  | 0.30 | 169.32 |  |  |  |  |  |  |
|  |  |  |  | 0.25 | 163.98 |  |  |  |  |  |  |
|  |  |  |  | 0.20 | 158.33 |  |  |  |  |  |  |
|  |  |  |  | 0.14 | 150.69 |  |  |  |  |  |  |

Table S2 Comparison of properties and CO2 capture capacities of state-of-the-art biochars.

| Feedstock | Pyrolysis | Activation method | CO2 adsorption (mg/g) | Adsorption conditions | BET surfaces area (m2/g) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Sludge | 600 °C, 1 h | - | 75.7 | 30 °C, 1 bar | 74.09 | [1] |
| Sludge | 600 °C, 1 h | K2FeO4 | 81.7 | 50 °C, 1 bar | 53.78 | [1] |
| Sludge | 600 °C, 1 h | K2FeO4 + Chitosan | 86.6 | 30 °C, 1 bar | 50.92 | [1] |
| Sludge | 600 °C, 1 h | K2FeO4 + cationicpolyacrylamide | 94.8 | 50 °C, 1 bar | 51.76 | [1] |
| Textile dyeing sludge and corncob | 700 °C, 2 h | K2CO3 | 128.1 | 25 °C, 1 bar | 544.38 | [2] |
| Corncob | 400 °C, 1.5 h | Copper nitrate | 103.3 (52.59 cm3/g) | 25 °C, 1 bar | 39.67 | [3] |
| Mixed food waste | 400 ℃, 1 h | KOH, 600 ℃, 1 h | 111.8 (2.54 mmol/g) | 25 °C, 1 bar | 807.00 | [4] |
| Pear branches | 600 ℃, 1 h | KOH, 650 ℃, 1 h | 155.8 | 0 °C, 1 bar | 1178.00 | [5] |
| Alfa Grass | 300 ℃ 2 h, 400 ℃ 2 h, 500 °C, 2 h | - | 52.8 (1.20 mmol/g) | 30 °C, 1 bar | 2.66 | [6] |
| Agave bagasse | 650 °C, 80 min | Ca(CH3COO)2·H2O | 106.5 (2.42 mmol/g) | 25 °C, 1 bar | 445.00 | [7] |
| Corn straw | 550 °C, 1 h | Ball milling, 450 rpm, 8 h | 45.4 | 30 °C, 1 bar | 80.90 | [8] |
| Banana stalk | 550 °C, 1 h | Ball milling, 450 rpm, 8 h | 49.9 | 30 °C, 1 bar | 4.80 | [8] |
| Cotton stalk | 550 °C, 1 h | Ball milling, 450 rpm, 8 h | 42.6 | 30 °C, 1 bar | 40.99 | [8] |
| Chinese herb residues | 700 °C, 1 h | K2CO3 | 69.1 (1.57 mmol/g) | 60 °C, 1 bar | 337.05 | [9] |
| Chinese herb residues | 700 °C, 1 h | K2CO3and K2FeO4 | 96.8 (2.20 mmol/g) | 60 °C, 1 bar | 420.54 | [9] |
| Pine wood | 700 °C, 2 h | CO2, 800 ℃, 2 h | 92.4 (2.10 mmol/g) | 25 °C, 1bar | 675.00 | [10] |
| Waste disposable chopsticks | 400 °C, 1 h | Melamine and FeCl3⋅6H2O | 157.5 (3.58 mmol/g) | 25 °C, 1 bar | 1315.90 | [11] |
| Bamboo | 600 °C, 5 h | Microwave irradiation | 134.5 | 0 °C, 1 bar | 377.32 | [12] |
| Olive pomace | 750 °C, 1 h | KOH | 40.0 | 10 °C, 1 bar | 1601.00 | [13] |
| Bagasse | 600 °C, 2 h | KOH | 165.4 (3.76 mmol/g) | 25 °C, 1 bar | 2559.92 | [14] |
| Rice husk | 700 °C, 2 h | Molten LiCl | 118.8 (2.70mmol/g) | 25 °C, 1 bar | 149.00 | [15] |
| Corncob | 800 °C, 1 h | K2CO3 and urea | 114.1 | 37 °C, 1 bar | 1016.26 | [16] |
| Wheat straw pellet | 500 °C, 1 h | CO2, 800 ℃, 1 h | 107.4 (2.44 mmol/g) | 25 °C, 1 bar | 514.00 | [17] |
| Pine needle | 500 °C, 2 h | KOH, 600 ℃, 2 h | 84.9 (1.93 mmol/g) | 40 °C, 1 bar | 504.81 | [18] |
| Wood pellets | 850 °C, 1 h | KOH, 850°C, 1 h | 50.7 | 25 °C, 1 bar | 713.50 | [19] |
| Sewage sludge | 600 °C, 1 h | Polymeric aluminum chloride | 31.9 | 30 °C, 1 bar | 41.21 | [20] |
| Sewage sludge | 600 °C, 1 h | Cationic polyacrylamide | 48.5 | 30 °C, 1 bar | 40.10 | [20] |
| Rice husk | 700 °C, 1 h | Potassium citrate | 68.2 (1.55 mmol/g) | 25 °C, 1 bar | 1343.80 | [21] |
| Corn stalk | 600 °C, 3 h | Sodium lignosulfonate | 102.9 | 0 °C, 1 bar | 118.14 | [22] |
| Soybean straw | 600 °C, 3 h | Sodium lignosulfonate | 89.8 | 0 °C, 1 bar | 257.65 | [22] |
| Sargassum | 800 °C, 2 h | KOH | 46.2 (1.05 mmol/g) | 25 °C, 1 bar | 291.80 | [23] |
| Sargassum | 400 °C, 2 h | KOH | 120.5 mg/g | 40 °C, 1 bar | 569.66 | This study |

Table S3 Chemical compositions of biochars calculated from XPS results.

| Sample | at.% C | at.% O | at.% N |
| --- | --- | --- | --- |
| SBC400 | 78.03 | 20.94 | 1.03 |
| SBC600 | 72.61 | 23.40 | 3.99 |
| SBC400-KOH | 74.05 | 24.02 | 1.92 |
| Sar-KOH | 82.78 | 15.65 | 1.57 |

Table S4 Compositions of C, O, and N species obtained by XPS surface analysis for biochars

| Sample | C |  |  |  |  |  |  |  |  |  |  |  |  |  |  | O |  |  |  |  |  |  | N |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C–C |  |  | C–N |  |  | C–O |  |  | C=O |  |  | O–C=O |  |  |  | O–H |  |  | C–O |  |  |  | Pyridinic N |  |  | Pyrrolic N |  |
|  | B.E. (eV) | % area |  | B.E. (eV) | % area |  | B.E. (eV) | % area |  | B.E. (eV) | % area |  | B.E. (eV) | % area |  |  | B.E. (eV) | % area |  | B.E. (eV) | % area |  |  | B.E. (eV) | % area |  | B.E. (eV) | % area |
| SBC400 | 284.79 | 78.0 |  | 286.19 | 10.1 |  | 287.29 | 4.4 |  | 288.69 | 7.5 |  | - | - |  |  | 531.69 | 78.8 |  | 533.49 | 21.2 |  |  | 398.69 | 40.3 |  | 400.19 | 59.7 |
| SBC600 | 284.80 | 68.6 |  | 285.70 | 11.2 |  | 286.80 | 9.0 |  | 288.20 | 6.3 |  | 289.40 | 4.8 |  |  | 531.80 | 78.6 |  | 533.40 | 21.4 |  |  | 398.40 | 49.1 |  | 400.30 | 50.9 |
| SBC400-KOH | 284.79 | 83.7 |  | - | - |  | 286.29 | 8.0 |  | 287.19 | 0.9 |  | 288.89 | 7.4 |  |  | 531.69 | 74.1 |  | 533.39 | 25.9 |  |  | 398.49 | 44.0 |  | 400.29 | 56.0 |
| Sar-KOH | 284.82 | 71.6 |  | - | - |  | 286.32 | 16.8 |  | 287.72 | 6.7 |  | 289.32 | 5.0 |  |  | 532.62 | 81.3 |  | 535.62 | 18.7 |  |  | 398.82 | 37.8 |  | 401.02 | 58.6 |

Table S5 CO2 adsorption capacities of the biocahrs

| Sample | SBC400 | SBC500 | SBC600 | SBC700 | SBC400-KOH | Sar-KOH |
| --- | --- | --- | --- | --- | --- | --- |
| CO2 adsorption capacity (mg/g) | 24.1 | 20.2 | 10.9 | 16.5 | 40.0 | 120.5 |
| CO2 adsorption capacity after 9 cycles (mg/g) | 20.0 | 18.9 | 10.6 | 15.1 | 37.2 | 119.2 |
| CO2 adsorption capacity after 18 cycles (mg/g) | 16.6 | 17.7 | 10.3 | 13.8 | 34.6 | 117.9 |
| Biochar requirement per kg CO2 (kg) | 2.73 | 2.93 | 5.24 | 3.67 | 1.49 | 0.47 |

References

[1]	Liu C, Fu C, Li T, Zhang P, Xia Y, et al. 2023. CO2 capture using biochar derived from conditioned sludge via pyrolysis. Separation and Purification Technology 314: 123624 https://doi.org/10.1016/j.seppur.2023.123624

[2]	Pan Y, Lei J, Zhang Z, Lou F, Song K, et al. 2025. CO2 capture performance of K2CO3-activated biochars derived from the textile dyeing sludge and corncob. Journal of CO2 Utilization 95: 103079 https://doi.org/10.1016/j.jcou.2025.103079

[3]	Gui H, Yang Z, Zhang Y, Huhe T, Li X. 2025. Construction of a floatable copper/corncob biochar composite with an LSPR effect for CO2 capture and efficient photothermal catalytic conversion. Inorganic Chemistry Frontiers 12: 7294-7303https://doi.org/10.1039/D5QI01217A

[4]	Yuan X, Wang J, Deng S, Dissanayake PD, Wang S, et al. 2022. Sustainable Food Waste Management: Synthesizing Engineered Biochar for CO2 Capture. ACS Sustainable Chemistry & Engineering 10: 13026-13036 https://doi.org/10.1021/acssuschemeng.2c03029

[5]	Di H, Zhang T, Ma H, Zhang G, Li K, et al. 2025. Biomass tar modified biochar with enhanced micropores and oxygen content for high efficiency CO2 capture. Separation and Purification Technology 378: 134678 https://doi.org/10.1016/j.seppur.2025.134678

[6]	Akaya H, Ouzrour Z, Aziz K, Golenarges S, Nakasu PYS, et al. 2025. Valorization of Moroccan Alfa Grass through Pyrolytic Conversion to Biochar for Atmospheric CO2 Capture. ACS Omega10:58991-59003https://doi.org/10.1021/acsomega.5c07867

[7]	Arjona-Jaime P, Morales-Ospino R, Izquierdo MT, Chazaro-Ruiz LF, Celzard A, et al. 2025. Ca-modified biochar by microwave irradiation for robust CO2 capture under realistic flue gas conditions. Chemical Engineering Journal 525: 170349 https://doi.org/10.1016/j.cej.2025.170349

[8]	Zhang P, Luo J, Huo L, Zhao L, Yao Z. 2025. Straw-derived porous biochars by ball milling for CO2 capture: Adsorption performance and enhanced mechanisms. Industrial Crops and Products 229: 121000 https://doi.org/10.1016/j.indcrop.2025.121000

[9]	Li Y, Guo Z, Qiu Y, Yang W, Lang L, et al. 2026. K-Fe based biochar granules prepared by one-step pyrolysis of herb-residue for stable CO2 capture: the importance of hydrophobic effect. Separation and Purification Technology 381: 135497 https://doi.org/10.1016/j.seppur.2025.135497

[10]	Abbaspour N, Jordan C, Tondl G, Wąsik P, Gholizadeh T, et al. 2025. Activated biochars from heavy metal-contaminated biomass for CO2 capture: Adsorption performance and dominant mechanisms. Journal of CO2 Utilization 101: 103217 https://doi.org/10.1016/j.jcou.2025.103217

[11]	Yin Q, Gao Y, Wang R, Zhu X, Gao X, et al. 2026. Influence of Fe-N co-doping on biochar on the adsorption of CO2. Chemical Engineering Science 320: 122702 https://doi.org/10.1016/j.ces.2025.122702

[12]	Zhang X, Xu H, Xiang W, You X, Dai H, et al. 2024. Lignin-impregnated biochar assisted with microwave irradiation for CO2 capture: adsorption performance and mechanism. Biochar 6: 22 https://doi.org/10.1007/s42773-024-00310-9

[13]	Monteagudo JM, Durán A, Alonso M, Stoica A-I. 2025. Investigation of effectiveness of KOH-activated olive pomace biochar for efficient direct air capture of CO2. Separation and Purification Technology 352: 127997 https://doi.org/10.1016/j.seppur.2024.127997

[14]	He G, Yuan X, Wang Y, Yilmaz M, Li J, et al. 2025. N, S-codoped porous biochar derived from bagasse-based polycondensate for high-performance CO2 capture and supercapacitor. Separation and Purification Technology 354: 128826 https://doi.org/10.1016/j.seppur.2024.128826

[15]	Li B, Li M, Xie X, Li C, Liu D. 2024. Pyrolysis of rice husk in molten lithium chloride: Biochar structure evolution and CO2 adsorption. Journal of the Energy Institute 113: 101526 https://doi.org/10.1016/j.joei.2024.101526

[16]	Li H, Tang M, Huang X, Wang L, Liu Q, et al. 2023. An efficient biochar adsorbent for CO2 capture: Combined experimental and theoretical study on the promotion mechanism of N-doping. Chemical Engineering Journal 466: 143095 https://doi.org/10.1016/j.cej.2023.143095

[17]	Manyà JJ, García-Morcate D, González B. 2020. Adsorption Performance of Physically Activated Biochars for Postcombustion CO2 Capture from Dry and Humid Flue Gas. Applied Sciences 10: 376 https://doi.org/10.3390/app10010376

[18]	Lim C, Jeong SG, Ha S, Ha N, Myeong S, et al. 2023. Unique CO2 adsorption of pine needle biochar-based activated carbons by induction of functionality transition. Journal of Industrial and Engineering Chemistry 124: 201-210https://doi.org/10.1016/j.jiec.2023.04.008

[19]	Zhang C, Sun S, Xu S, Wu C. 2022. CO2 capture over steam and KOH activated biochar: Effect of relative humidity. Biomass and Bioenergy 166: 106608https://doi.org/10.1016/j.biombioe.2022.106608

[20]	Liu C, Wu Y, Lan G, Ji X, Xia Y, et al. 2022. CO2 capture performance of biochar prepared from sewage sludge after conditioning with different dewatering agents. Journal of Environmental Chemical Engineering 10: 108318 https://doi.org/10.1016/j.jece.2022.108318

[21]	Gan F, Wang B, Guo J, He J, Ma S, et al. 2022. Green synthesis of porous biochar with interconnected pore architectures from typical silicon-rich rice husk for efficient CO2 capture. Separation and Purification Technology 302: 122089 https://doi.org/10.1016/j.seppur.2022.122089

[22]	Zhang X, Cao L, Xiang W, Xu Y, Gao B. 2022. Preparation and evaluation of fine-tuned micropore biochar by lignin impregnation for CO2 and VOCs adsorption. Separation and Purification Technology 295: 121295 https://doi.org/10.1016/j.seppur.2022.121295

[23]	Ding S, Liu Y. 2020. Adsorption of CO2 from flue gas by novel seaweed-based KOH-activated porous biochars. Fuel 260: 116382 https://doi.org/10.1016/j.fuel.2019.116382