Elemental composition-based prediction of persistent free radicals concentration and g-Factor in lignocellulose-derived biochar combining interpretable machine learning and experimental analysis

Linjian Gao , Chengcheng Xu , Mengzi Li , Zhongda Xu , Wenmei Tao *

Faculty of Modern Agricultural Engineering, Kunming University of Science & Technology, Kunming 650500, Yunnan, China.

Corresponding author: Wenmei Tao, Email: taowenmei123@163.com

Fig. S1 IQR-based boxplot.

Fig. S2 ROC curve analysis of different machine-learning models for PFRs concentration.

Fig. S3 ROC curve analysis of different machine-learning models for g-Factor.

Fig. S4 Conditional PDP analysis of H for g-Factor based on similar O/C.

Fig. S5 SHAP interaction heatmap.

Fig. S6 Linear relationship between elemental composition and PFRs concentration: (a) C, (b) H/C, (c) H, (d) O, (e) O/C.

Fig. S7 linear relationship between elemental composition and g-Factor: (a) C, (b) H/C, (c) H, (d) O, (e) O/C.

Fig. S8 The relationship between H/C and PFRs signal: (a) CL, (b) LG, (c) PH.

Fig. S9 3D scatter plots of O/C, H, and g-Factor.

Fig. S10 Spearman correlation validation between elemental composition and PFRs: (a) concentration, (b) g-Factor.

Table S1 Machine learning dataset

| Biomass | H | O | O/C | H/C | C | contents(1020 Spins/g) | g-Factor value | Source |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Corncob | 4.24 | 4.19 | 0.14 | 0.69 | 73.94 | 0.7366 | 2.0030 | [1] |
| Corncob | 4.19 | 4.14 | 0.13 | 0.68 | 73.94 | 0.8455 | 2.0029 |  |
| Corncob | 4.02 | 3.95 | 0.11 | 0.64 | 75.54 | 1.0974 | 2.0028 |  |
| Corncob | 3.73 | 3.73 | 0.09 | 0.60 | 74.46 | 1.4047 | 2.0027 |  |
| Corncob | 3.19 | 3.19 | 0.07 | 0.53 | 72.05 | 2.0651 | 2.0026 |  |
| Corncob | 3.09 | 3.09 | 0.07 | 0.51 | 72.00 | 2.1901 | 2.0025 |  |
| Corncob | 1.81 | 1.81 | 0.06 | 0.34 | 63.82 | 1.8366 | 2.0024 |  |
| Corncob | 1.78 | 1.78 | 0.05 | 0.32 | 66.68 | 1.6667 | 2.0024 |  |
| Coconut shell | 2.91 | 24.54 | 0.43 | 0.85 | 41.06 | 0.1849 | 2.0033 |  |
| Coconut shell | 2.70 | 22.99 | 0.38 | 0.74 | 43.85 | 0.3513 | 2.0032 |  |
| Coconut shell | 2.51 | 21.46 | 0.35 | 0.72 | 41.66 | 0.4338 | 2.0031 |  |
| Coconut shell | 2.42 | 20.71 | 0.32 | 0.69 | 41.93 | 0.4884 | 2.0030 |  |
| Coconut shell | 2.35 | 19.97 | 0.31 | 0.63 | 44.63 | 0.6413 | 2.0030 |  |
| Coconut shell | 2.28 | 19.25 | 0.27 | 0.61 | 45.19 | 0.7605 | 2.0029 |  |
| Coconut shell | 2.12 | 17.19 | 0.24 | 0.57 | 44.83 | 1.1312 | 2.0028 |  |
| Coconut shell | 2.07 | 16.54 | 0.23 | 0.56 | 44.11 | 1.2650 | 2.0027 |  |
| Coconut shell | 2.03 | 15.92 | 0.22 | 0.55 | 44.57 | 1.3827 | 2.0027 |  |
| Coconut shell | 1.78 | 13.24 | 0.19 | 0.48 | 44.72 | 1.8682 | 2.0026 |  |
| Coconut shell | 1.25 | 10.18 | 0.14 | 0.34 | 44.57 | 2.1142 | 2.0025 |  |
| Coconut shell | 1.18 | 9.82 | 0.13 | 0.32 | 43.75 | 2.0147 | 2.0024 |  |
| Coconut shell | 0.44 | 3.79 | 0.04 | 0.12 | 43.65 | 0.2510 | 2.0024 |  |
| Bamboo wood | 3.35 | 13.80 | 0.22 | 0.82 | 48.86 | 0.8203 | 2.0030 |  |
| Bamboo wood | 3.28 | 13.27 | 0.21 | 0.79 | 49.62 | 0.8338 | 2.0029 |  |
| Bamboo wood | 2.95 | 9.79 | 0.17 | 0.70 | 50.85 | 1.0184 | 2.0028 | [1] |
| Bamboo wood | 2.85 | 8.63 | 0.16 | 0.69 | 49.68 | 1.0657 | 2.0027 |  |
| Bamboo wood | 2.24 | 3.93 | 0.08 | 0.69 | 39.00 | 1.5847 | 2.0026 |  |
| Bamboo wood | 0.97 | 1.66 | 0.03 | 0.21 | 55.27 | 0.7176 | 2.0025 |  |
| Rice straw | 3.23 | 17.63 | 0.29 | 0.80 | 48.60 | 0.3983 | 2.0032 |  |
| Rice straw | 3.09 | 16.49 | 0.28 | 0.76 | 49.10 | 0.4516 | 2.0031 |  |
| Rice straw | 2.47 | 12.66 | 0.24 | 0.61 | 48.67 | 0.8629 | 2.0030 |  |
| Rice straw | 2.06 | 11.62 | 0.22 | 0.51 | 48.91 | 1.3895 | 2.0029 |  |
| Rice straw | 1.77 | 10.68 | 0.19 | 0.45 | 47.44 | 2.0938 | 2.0028 |  |
| Rice straw | 1.42 | 10.68 | 0.18 | 0.35 | 48.91 | 1.7248 | 2.0027 |  |
| Rice straw | 0.89 | 6.43 | 0.15 | 0.21 | 51.49 | 0.4623 | 2.0026 |  |
| Rice husk | 4.15 | 16.23 | 0.23 | 0.96 | 51.75 | 0.3610 | 2.0032 |  |
| Rice husk | 4.10 | 16.06 | 0.23 | 0.95 | 52.06 | 0.4273 | 2.0031 |  |
| Rice husk | 3.99 | 15.63 | 0.23 | 0.92 | 51.99 | 0.4540 | 2.0031 |  |
| Rice husk | 3.39 | 13.24 | 0.23 | 0.81 | 50.23 | 0.6607 | 2.0030 |  |
| Rice husk | 2.81 | 11.95 | 0.22 | 0.70 | 48.42 | 0.9583 | 2.0029 |  |
| Rice husk | 2.25 | 13.06 | 0.20 | 0.55 | 48.96 | 1.4001 | 2.0028 |  |
| Rice husk | 1.32 | 10.78 | 0.17 | 0.34 | 46.61 | 1.4554 | 2.0027 |  |
| Rice husk | 0.81 | 9.87 | 0.16 | 0.21 | 45.66 | 0.6384 | 2.0026 |  |
| Pine wood | 4.40 | 23.49 | 0.27 | 0.80 | 65.88 | 0.4314 | 2.0033 |  |
| Pine wood | 4.14 | 21.68 | 0.26 | 0.78 | 63.71 | 0.4581 | 2.0032 |  |
| Pine wood | 3.97 | 20.95 | 0.23 | 0.73 | 65.64 | 0.5042 | 2.0031 |  |
| Pine wood | 3.82 | 19.81 | 0.22 | 0.68 | 66.93 | 0.5309 | 2.0030 |  |
| Pine wood | 3.26 | 15.46 | 0.16 | 0.54 | 73.01 | 0.8926 | 2.0029 |  |
| Pine wood | 3.15 | 14.83 | 0.15 | 0.53 | 71.28 | 0.9986 | 2.0028 | [1] |
| Pine wood | 2.73 | 11.62 | 0.12 | 0.43 | 76.61 | 1.9645 | 2.0027 |  |
| Pine wood | 1.42 | 3.01 | 0.03 | 0.20 | 83.54 | 0.5562 | 2.0026 |  |
| Woody | 4.14 | 4.09 | 0.12 | 0.67 | 74.40 | 0.9339 | 2.0029 | [2] |
| Woody | 3.95 | 3.95 | 0.10 | 0.61 | 77.79 | 1.2723 | 2.0028 |  |
| Woody | 3.32 | 3.32 | 0.08 | 0.54 | 73.97 | 1.9401 | 2.0026 |  |
| Woody | 2.83 | 2.83 | 0.07 | 0.49 | 69.40 | 2.4167 | 2.0025 |  |
| Woody | 2.41 | 2.41 | 0.06 | 0.42 | 68.23 | 2.7323 | 2.0025 |  |
| Woody | 2.13 | 2.13 | 0.06 | 0.37 | 69.32 | 2.4899 | 2.0025 |  |
| Woody | 1.64 | 1.64 | 0.05 | 0.31 | 63.20 | 1.3650 | 2.0024 |  |
| Woody | 1.37 | 1.37 | 0.04 | 0.25 | 64.78 | 1.0199 | 2.0024 |  |
| Woody | 0.99 | 0.99 | 0.02 | 0.17 | 68.27 | 0.9363 | 2.0024 |  |
| Sludge | 3.23 | 12.72 | 0.20 | 0.78 | 49.90 | 0.8840 | 2.0029 | [3] |
| sludge | 3.11 | 11.57 | 0.19 | 0.72 | 51.64 | 0.9462 | 2.0028 |  |
| Sludge | 2.61 | 5.86 | 0.11 | 0.61 | 51.41 | 1.2826 | 2.0027 |  |
| Sludge | 2.17 | 3.85 | 0.07 | 0.66 | 39.48 | 1.6701 | 2.0025 |  |
| Sludge | 2.10 | 3.78 | 0.06 | 0.63 | 40.00 | 1.8277 | 2.0025 |  |
| Sludge | 1.59 | 2.58 | 0.05 | 0.49 | 38.98 | 1.7697 | 2.0025 |  |
| Sludge | 0.99 | 1.76 | 0.03 | 0.21 | 56.25 | 0.7217 | 2.0025 |  |
| Hard wood | 4.07 | 21.16 | 0.24 | 0.75 | 65.45 | 0.4834 | 2.0032 | [4] |
| Hard wood | 3.56 | 18.36 | 0.19 | 0.63 | 67.35 | 0.5814 | 2.0030 |  |
| Hard wood | 3.41 | 17.12 | 0.17 | 0.57 | 71.46 | 0.7247 | 2.0029 |  |
| Hard wood | 2.95 | 13.17 | 0.14 | 0.50 | 71.10 | 1.2912 | 2.0028 |  |
| Hard wood | 2.44 | 9.75 | 0.10 | 0.38 | 77.50 | 2.2577 | 2.0027 |  |
| Hard wood | 2.06 | 7.78 | 0.09 | 0.32 | 77.52 | 1.7045 | 2.0026 |  |
| Hard wood | 1.48 | 3.73 | 0.04 | 0.21 | 84.13 | 0.5882 | 2.0026 |  |
| Woody | 2.80 | 23.77 | 0.40 | 0.80 | 42.22 | 0.2659 | 2.0033 | [5] |
| Woody | 2.22 | 18.53 | 0.26 | 0.60 | 44.67 | 0.8855 | 2.0029 |  |
| Woody | 2.01 | 15.33 | 0.22 | 0.52 | 46.41 | 1.5092 | 2.0027 |  |
| Woody | 1.91 | 14.23 | 0.20 | 0.50 | 45.58 | 1.6431 | 2.0026 |  |
| Woody | 1.72 | 12.77 | 0.18 | 0.46 | 44.76 | 1.9698 | 2.0025 |  |
| Woody | 1.52 | 11.53 | 0.16 | 0.40 | 45.93 | 2.1849 | 2.0025 |  |
| Woody | 1.45 | 11.20 | 0.16 | 0.38 | 46.11 | 2.2087 | 2.0025 |  |
| Woody | 0.71 | 7.26 | 0.08 | 0.20 | 43.04 | 1.2050 | 2.0024 |  |
| Woody | 0.46 | 4.13 | 0.04 | 0.12 | 44.05 | 0.3373 | 2.0024 |  |
| Woody | 3.32 | 19.62 | 0.31 | 0.83 | 47.73 | 0.3315 | 2.0032 |  |
| Woody | 2.89 | 15.56 | 0.27 | 0.74 | 46.92 | 0.5181 | 2.0031 |  |
| Woody | 2.85 | 15.25 | 0.26 | 0.70 | 48.77 | 0.5977 | 2.0030 |  |
| Woody | 2.56 | 13.28 | 0.24 | 0.64 | 47.81 | 0.7039 | 2.0030 |  |
| Woody | 2.29 | 12.34 | 0.23 | 0.58 | 47.65 | 0.9850 | 2.0029 |  |
| Woody | 1.83 | 11.00 | 0.19 | 0.45 | 48.56 | 1.9879 | 2.0028 |  |
| Woody | 1.59 | 11.20 | 0.18 | 0.39 | 48.44 | 2.2005 | 2.0027 |  |
| Woody | 0.92 | 7.26 | 0.16 | 0.22 | 50.45 | 0.5011 | 2.0026 |  |
| Woody | 3.58 | 13.99 | 0.23 | 0.83 | 51.78 | 0.6017 | 2.0030 |  |
| Woody | 1.99 | 12.57 | 0.20 | 0.50 | 47.88 | 1.6505 | 2.0027 |  |
| Woody | 1.25 | 10.46 | 0.17 | 0.32 | 47.00 | 1.2476 | 2.0026 |  |
| Corncob | 1.31 | 10.52 | 0.15 | 0.35 | 45.19 | 2.1726 | 2.0025 | [6] |
| Corncob | 0.84 | 8.09 | 0.10 | 0.23 | 44.23 | 1.4759 | 2.0024 |  |
| Corncob | 1.03 | 9.23 | 0.12 | 0.28 | 43.91 | 1.7747 | 2.0024 |  |
| Corncob | 0.65 | 6.43 | 0.07 | 0.17 | 45.55 | 0.9400 | 2.0024 |  |
| Corncob | 0.54 | 5.15 | 0.06 | 0.14 | 45.86 | 0.6152 | 2.0024 |  |
| Pine wood | 1.16 | 9.85 | 0.18 | 0.30 | 46.78 | 1.0406 | 2.0026 |  |
| Pine wood | 1.28 | 10.68 | 0.18 | 0.34 | 45.29 | 1.4932 | 2.0026 |  |
| Pine wood | 1.04 | 8.91 | 0.17 | 0.25 | 49.27 | 0.6849 | 2.0026 |  |
| Pine wood | 2.57 | 11.17 | 0.21 | 0.64 | 48.00 | 1.1233 | 2.0028 |  |
| Pine wood | 1.63 | 11.73 | 0.19 | 0.41 | 48.23 | 1.7708 | 2.0027 |  |
| Bagasse | 1.03 | 10.14 | 0.16 | 0.26 | 47.51 | 0.9568 | 2.0026 |  |
| Bagasse | 1.89 | 6.12 | 0.07 | 0.28 | 81.72 | 1.2256 | 2.0026 |  |
| Bagasse | 1.55 | 4.67 | 0.05 | 0.23 | 81.61 | 0.6712 | 2.0026 |  |
| Bagasse | 3.50 | 3.50 | 0.09 | 0.57 | 73.24 | 1.6738 | 2.0026 |  |
| Bagasse | 2.22 | 2.22 | 0.06 | 0.39 | 67.54 | 2.6801 | 2.0025 |  |
| Rice husk | 1.55 | 1.55 | 0.04 | 0.28 | 66.08 | 1.1514 | 2.0024 |  |
| Rice husk | 1.13 | 1.13 | 0.02 | 0.21 | 65.23 | 0.9430 | 2.0024 |  |
| Maize straw | 1.91 | 3.32 | 0.05 | 0.57 | 40.42 | 1.9578 | 2.0025 |  |
| Maize straw | 1.23 | 2.28 | 0.04 | 0.28 | 52.40 | 0.9544 | 2.0025 |  |
| Coconut shell | 2.78 | 12.03 | 0.12 | 0.44 | 75.84 | 1.8072 | 2.0028 |  |
| Enteromorpha | 1.71 | 6.12 | 0.06 | 0.25 | 80.86 | 0.8758 | 2.0026 |  |
| Rice straw | 4.09 | 4.02 | 0.12 | 0.66 | 74.87 | 1.0369 | 2.0028 | [7] |
| Rice straw | 3.56 | 3.56 | 0.09 | 0.59 | 72.57 | 1.5385 | 2.0027 |  |
| Rice straw | 3.39 | 3.39 | 0.08 | 0.55 | 73.78 | 1.8092 | 2.0026 |  |
| Rice straw | 2.95 | 2.95 | 0.07 | 0.50 | 70.53 | 2.3621 | 2.0025 |  |
| Rice straw | 2.73 | 2.73 | 0.07 | 0.48 | 68.05 | 2.5198 | 2.0025 |  |
| Rice straw | 2.64 | 2.64 | 0.07 | 0.46 | 68.29 | 2.6022 | 2.0025 |  |
| Rice straw | 2.58 | 2.58 | 0.06 | 0.46 | 67.74 | 2.6686 | 2.0025 |  |
| Pine wood | 2.51 | 2.51 | 0.06 | 0.44 | 67.79 | 2.7114 | 2.0025 |  |
| Pine wood | 2.32 | 2.32 | 0.06 | 0.41 | 67.12 | 2.7194 | 2.0025 |  |
| Pine wood | 2.17 | 2.17 | 0.06 | 0.38 | 68.89 | 2.5938 | 2.0025 |  |
| Pine wood | 2.08 | 2.08 | 0.06 | 0.36 | 70.02 | 2.3479 | 2.0025 |  |
| Pine wood | 2.00 | 2.00 | 0.06 | 0.35 | 67.95 | 2.1897 | 2.0025 |  |
| Pine wood | 1.67 | 1.67 | 0.05 | 0.32 | 62.85 | 1.5085 | 2.0024 |  |
| Pine wood | 1.59 | 1.59 | 0.04 | 0.29 | 65.61 | 1.2464 | 2.0024 |  |
| Pine wood | 1.40 | 1.40 | 0.04 | 0.25 | 66.39 | 1.0797 | 2.0024 |  |
| Pine wood | 1.33 | 1.33 | 0.03 | 0.22 | 71.34 | 0.9820 | 2.0024 |  |
| Pine wood | 1.18 | 1.18 | 0.03 | 0.22 | 65.57 | 0.9574 | 2.0024 |  |
| Pine wood | 1.06 | 1.06 | 0.02 | 0.20 | 63.85 | 0.9375 | 2.0024 |  |
| Pine wood | 1.03 | 1.03 | 0.02 | 0.19 | 65.91 | 0.9363 | 2.0024 |  |
| Sewage sludge | 3.18 | 12.16 | 0.19 | 0.76 | 50.45 | 0.9313 | 2.0029 | [8] |
| Sewage sludge | 2.75 | 7.47 | 0.13 | 0.64 | 51.30 | 1.1676 | 2.0027 |  |
| Sewage sludge | 2.44 | 4.68 | 0.09 | 0.57 | 51.57 | 1.4212 | 2.0026 |  |
| Sewage sludge | 1.74 | 2.85 | 0.06 | 0.51 | 40.68 | 1.9187 | 2.0025 |  |
| Sewage sludge | 1.39 | 14.63 | 0.05 | 0.44 | 37.46 | 1.4022 | 2.0025 |  |
| Sewage sludge | 1.11 | 2.18 | 0.04 | 0.25 | 53.60 | 0.7836 | 2.0025 |  |
| Corn stalks | 2.10 | 11.72 | 0.22 | 0.51 | 49.05 | 1.2586 | 2.0029 | [9] |
| Bamboo | 2.00 | 11.51 | 0.21 | 0.49 | 49.09 | 1.5556 | 2.0028 |  |
| Pig manure | 1.90 | 11.31 | 0.20 | 0.47 | 48.59 | 1.8791 | 2.0028 |  |
| Pig manure | 1.57 | 11.00 | 0.18 | 0.39 | 48.78 | 2.1450 | 2.0027 |  |
| Laminaria | 1.23 | 10.27 | 0.18 | 0.32 | 46.31 | 1.2119 | 2.0026 | [10] |
| Laminaria | 1.13 | 9.82 | 0.17 | 0.28 | 48.71 | 0.8692 | 2.0026 |  |
| Laminaria | 1.10 | 9.50 | 0.17 | 0.27 | 48.77 | 0.8033 | 2.0026 |  |
| Laminaria | 0.99 | 8.09 | 0.16 | 0.23 | 51.31 | 0.5798 | 2.0026 |  |
| Cigarettes | 3.88 | 15.18 | 0.23 | 0.90 | 51.68 | 0.4984 | 2.0031 | [11] |
| Cigarettes | 3.08 | 12.57 | 0.22 | 0.76 | 48.89 | 0.8007 | 2.0029 |  |
| Cigarettes | 2.93 | 12.31 | 0.22 | 0.72 | 48.94 | 0.8773 | 2.0029 |  |
| Cigarettes | 2.43 | 13.24 | 0.20 | 0.59 | 49.51 | 1.2058 | 2.0028 |  |
| Cigarettes | 2.32 | 13.15 | 0.20 | 0.57 | 48.65 | 1.3073 | 2.0028 |  |
| Cigarettes | 2.09 | 12.92 | 0.20 | 0.54 | 46.75 | 1.4928 | 2.0027 |  |
| Cigarettes | 2.02 | 12.75 | 0.20 | 0.51 | 47.04 | 1.5753 | 2.0027 |  |
| Cigarettes | 1.91 | 12.31 | 0.19 | 0.44 | 52.04 | 1.7567 | 2.0027 |  |
| Cigarettes | 1.80 | 12.16 | 0.19 | 0.43 | 50.40 | 1.7834 | 2.0027 |  |
| Cigarettes | 1.49 | 11.36 | 0.18 | 0.38 | 46.97 | 1.6849 | 2.0027 |  |
| Cigarettes | 1.46 | 11.17 | 0.18 | 0.37 | 46.91 | 1.6147 | 2.0027 |  |
| Cigarettes | 1.15 | 10.29 | 0.16 | 0.29 | 47.02 | 1.1132 | 2.0026 |  |
| Cigarettes | 0.95 | 9.99 | 0.16 | 0.24 | 48.18 | 0.8121 | 2.0026 |  |
| Rice straw | 3.50 | 17.84 | 0.19 | 0.61 | 68.76 | 0.6243 | 2.0029 | [12] |
| Rice straw | 2.90 | 12.76 | 0.13 | 0.48 | 72.28 | 1.4617 | 2.0028 |  |
| Rice straw | 2.86 | 12.55 | 0.13 | 0.46 | 73.98 | 1.6337 | 2.0028 |  |
| Rice straw | 2.54 | 10.48 | 0.11 | 0.40 | 75.76 | 2.1867 | 2.0027 |  |
| Rice straw | 2.32 | 9.23 | 0.10 | 0.36 | 77.10 | 2.1263 | 2.0026 |  |
| Rice straw | 2.29 | 8.92 | 0.09 | 0.35 | 78.68 | 2.0033 | 2.0026 |  |
| Rice straw | 1.98 | 7.05 | 0.08 | 0.29 | 80.60 | 1.4365 | 2.0026 |  |
| Rice straw | 2.80 | 8.06 | 0.15 | 0.66 | 50.94 | 1.1115 | 2.0027 |  |
| Rice straw | 2.66 | 6.35 | 0.12 | 0.63 | 50.69 | 1.2222 | 2.0027 |  |
| Rice straw | 2.56 | 5.41 | 0.10 | 0.59 | 52.55 | 1.3446 | 2.0026 |  |
| Rice straw | 2.34 | 4.21 | 0.08 | 0.70 | 40.29 | 1.5007 | 2.0026 |  |
| Rice straw | 2.14 | 3.83 | 0.07 | 0.64 | 39.86 | 1.7511 | 2.0025 |  |
| Rice straw | 2.07 | 3.67 | 0.06 | 0.61 | 40.68 | 1.8926 | 2.0025 |  |
| Rice straw | 1.98 | 3.41 | 0.06 | 0.59 | 40.67 | 1.9443 | 2.0025 |  |
| Rice straw | 1.80 | 2.95 | 0.06 | 0.53 | 40.88 | 1.9566 | 2.0025 |  |
| Rice straw | 3.26 | 17.95 | 0.29 | 0.82 | 47.86 | 0.3584 | 2.0032 | [13] |
| Rice straw | 2.62 | 13.49 | 0.25 | 0.67 | 46.98 | 0.7038 | 2.0030 |  |
| Rice straw | 2.25 | 12.03 | 0.23 | 0.57 | 47.55 | 1.0895 | 2.0029 |  |
| Rice straw | 1.95 | 11.31 | 0.20 | 0.48 | 48.94 | 1.7130 | 2.0028 |  |
| Corn straw | 1.70 | 10.37 | 0.19 | 0.42 | 48.61 | 2.1867 | 2.0027 |  |
| Corn straw | 1.68 | 10.27 | 0.18 | 0.41 | 49.59 | 2.2266 | 2.0027 |  |
| Corn straw | 1.44 | 10.89 | 0.18 | 0.36 | 47.79 | 1.8595 | 2.0027 |  |
| Corn straw | 1.25 | 10.37 | 0.18 | 0.33 | 45.76 | 1.3438 | 2.0026 |  |
| Corn straw | 1.22 | 10.06 | 0.18 | 0.30 | 48.17 | 1.1328 | 2.0026 |  |
| Soft wood | 1.15 | 9.85 | 0.18 | 0.29 | 48.10 | 0.9747 | 2.0026 |  |
| Soft wood | 1.05 | 9.23 | 0.17 | 0.26 | 47.97 | 0.7375 | 2.0026 |  |
| Soft wood | 1.03 | 8.51 | 0.17 | 0.24 | 52.14 | 0.6059 | 2.0026 |  |
| Soft wood | 0.98 | 7.68 | 0.16 | 0.22 | 53.28 | 0.5008 | 2.0026 |  |
| Hard wood | 0.91 | 6.85 | 0.16 | 0.22 | 50.47 | 0.4619 | 2.0026 |  |
| Hard wood | 3.77 | 14.70 | 0.23 | 0.88 | 51.24 | 0.5618 | 2.0030 |  |
| Hard wood | 3.26 | 13.06 | 0.22 | 0.78 | 50.39 | 0.7314 | 2.0029 |  |
| Crop | 2.75 | 11.73 | 0.21 | 0.66 | 50.02 | 1.0408 | 2.0028 | [14] |
| Crop | 2.17 | 17.84 | 0.25 | 0.58 | 45.21 | 1.0091 | 2.0028 |  |
| Crop | 1.84 | 13.72 | 0.19 | 0.49 | 45.16 | 1.7505 | 2.0026 |  |
| Crop | 1.66 | 12.30 | 0.18 | 0.44 | 44.79 | 2.0610 | 2.0025 |  |
| Crop | 1.59 | 11.87 | 0.17 | 0.41 | 46.06 | 2.1318 | 2.0025 |  |
| Crop | 1.38 | 10.87 | 0.15 | 0.36 | 46.37 | 2.2075 | 2.0025 |  |
| Crop | 1.11 | 9.50 | 0.13 | 0.31 | 43.24 | 1.8976 | 2.0024 |  |
| Firewood | 0.91 | 8.51 | 0.11 | 0.26 | 42.33 | 1.6297 | 2.0024 |  |
| Firewood | 0.77 | 7.68 | 0.09 | 0.21 | 44.50 | 1.3427 | 2.0024 |  |
| Firewood | 0.68 | 6.85 | 0.08 | 0.18 | 44.58 | 1.0659 | 2.0024 |  |
| Firewood | 0.61 | 6.03 | 0.07 | 0.16 | 46.39 | 0.8229 | 2.0024 |  |
| Firewood | 0.57 | 5.60 | 0.06 | 0.15 | 47.23 | 0.7176 | 2.0024 |  |
| Firewood | 0.51 | 4.76 | 0.05 | 0.13 | 46.13 | 0.5127 | 2.0024 |  |
| Firewood | 0.48 | 4.45 | 0.05 | 0.13 | 43.71 | 0.4250 | 2.0024 |  |
| Coal | 1.52 | 2.48 | 0.05 | 0.48 | 38.29 | 1.6467 | 2.0025 |  |
| Coal | 1.51 | 2.37 | 0.05 | 0.46 | 39.22 | 1.5281 | 2.0025 |  |
| Coal | 1.35 | 2.18 | 0.05 | 0.41 | 39.09 | 1.2793 | 2.0025 |  |
| Coal | 1.28 | 1.97 | 0.04 | 0.40 | 38.66 | 1.1534 | 2.0025 |  |
| Coal | 1.28 | 1.97 | 0.04 | 0.39 | 39.48 | 1.0539 | 2.0025 |  |
| Coal | 1.21 | 2.28 | 0.04 | 0.27 | 54.05 | 0.8784 | 2.0025 |  |
| Coal | 1.15 | 2.28 | 0.04 | 0.26 | 52.61 | 0.8626 | 2.0025 |  |
| Rice husk | 3.72 | 19.40 | 0.20 | 0.65 | 68.46 | 0.5562 | 2.0030 | [15] |
| Rice husk | 3.43 | 17.43 | 0.18 | 0.60 | 68.83 | 0.6774 | 2.0029 |  |
| Rice husk | 3.31 | 15.77 | 0.17 | 0.56 | 71.39 | 0.8028 | 2.0029 |  |
| Rice husk | 3.02 | 13.80 | 0.14 | 0.51 | 70.40 | 1.1309 | 2.0028 |  |
| Rice husk | 2.68 | 11.31 | 0.11 | 0.41 | 78.22 | 2.1013 | 2.0027 |  |
| Rice husk | 2.51 | 10.17 | 0.11 | 0.39 | 76.32 | 2.2486 | 2.0027 |  |
| Rice husk | 2.37 | 9.54 | 0.10 | 0.37 | 77.03 | 2.2155 | 2.0027 |  |
| Rice husk | 2.18 | 8.30 | 0.09 | 0.33 | 78.92 | 1.8583 | 2.0026 |  |
| Rice husk | 2.03 | 7.47 | 0.08 | 0.31 | 79.32 | 1.5390 | 2.0026 |  |
| Rice husk | 1.93 | 6.64 | 0.08 | 0.29 | 80.79 | 1.3442 | 2.0026 |  |
| Rice husk | 1.77 | 6.64 | 0.07 | 0.27 | 78.93 | 0.9753 | 2.0026 |  |
| Rice husk | 1.65 | 5.60 | 0.05 | 0.25 | 79.74 | 0.7968 | 2.0026 |  |
| Rice husk | 1.60 | 5.19 | 0.05 | 0.24 | 81.34 | 0.7267 | 2.0026 |  |
| Rice husk | 1.52 | 4.15 | 0.04 | 0.22 | 82.82 | 0.6290 | 2.0026 |  |
| Rice husk | 1.95 | 12.44 | 0.20 | 0.48 | 48.64 | 1.7124 | 2.0027 |  |
| Rice husk | 1.63 | 11.95 | 0.19 | 0.41 | 47.16 | 1.7867 | 2.0027 |  |
| Rice husk | 1.58 | 11.55 | 0.19 | 0.39 | 47.97 | 1.7286 | 2.0027 |  |
| Rice husk | 1.39 | 10.98 | 0.18 | 0.35 | 47.78 | 1.5284 | 2.0027 |  |
| Rice husk | 1.30 | 10.53 | 0.17 | 0.33 | 47.61 | 1.3530 | 2.0026 |  |
| Rice husk | 1.20 | 10.37 | 0.16 | 0.31 | 46.13 | 1.1936 | 2.0026 |  |
| Rice husk | 1.07 | 10.22 | 0.16 | 0.27 | 46.92 | 1.0343 | 2.0026 |  |
| Rice husk | 1.00 | 10.06 | 0.16 | 0.25 | 47.17 | 0.8852 | 2.0026 |  |
| Rice husk | 0.91 | 9.94 | 0.15 | 0.23 | 47.93 | 0.7478 | 2.0026 |  |
| Rice husk | 0.86 | 9.90 | 0.16 | 0.22 | 46.28 | 0.6733 | 2.0026 |  |
| Rice husk | 1.08 | 1.97 | 0.04 | 0.24 | 54.68 | 0.7516 | 2.0025 |  |
| Rice husk | 1.04 | 1.87 | 0.04 | 0.23 | 53.90 | 0.7329 | 2.0025 |  |
| Rice husk | 1.01 | 1.76 | 0.03 | 0.22 | 55.08 | 0.7200 | 2.0025 |  |
| Rice husk | 1.66 | 2.73 | 0.05 | 0.50 | 39.65 | 1.8574 | 2.0025 |  |
| Bamboo | 4.98 | 14.58 | 0.14 | 35.13 | 1.70 | 0.0794 | 2.0026 | [16] |
| Corn stalks | 4.53 | 19.14 | 0.18 | 50.70 | 1.07 | 0.0967 | 2.0029 |  |
| Pig manure | 3.68 | 11.64 | 0.12 | 37.96 | 1.16 | 0.1413 | 2.0028 |  |
| Pig manure | 1.96 | 17.47 | 0.36 | 0.65 | 36.17 | 0.0745 | 2.0044 | [17] |
| Pig manure | 1.45 | 14.21 | 0.32 | 0.52 | 33.36 | 0.1396 | 2.0041 |  |
| Pig manure | 0.67 | 5.36 | 0.14 | 0.28 | 28.71 | 0.1123 | 2.0034 |  |
| Cellulose | 3.53 | 18.46 | 0.21 | 0.64 | 65.90 | 0.0163 | 2.0040 | [18] |
| Cellulose | 3.20 | 16.47 | 0.18 | 0.56 | 68.59 | 0.0193 | 2.0038 |  |
| Cellulose | 2.89 | 15.27 | 0.16 | 0.50 | 70.06 | 0.0121 | 2.0004 |  |
| Cellulose | 2.73 | 13.95 | 0.14 | 0.45 | 72.84 | 0.0201 | 2.0036 |  |
| Cellulose | 2.43 | 12.74 | 0.13 | 0.39 | 75.04 | 0.0173 | 2.0036 |  |
| Pine needles | 6.43 | 26.20 | 0.30 | 1.19 | 65.10 | 0.0538 | 2.0044 | [19] |
| Pine needles | 5.16 | 25.20 | 0.28 | 0.92 | 67.60 | 0.1520 | 2.0037 |  |
| Pine needles | 4.38 | 19.70 | 0.20 | 0.71 | 73.60 | 0.2230 | 2.0032 |  |
| Wheat straw | 6.10 | 30.90 | 0.38 | 1.19 | 61.50 | 0.0368 | 2.0042 |  |
| Wheat straw | 4.32 | 25.80 | 0.28 | 0.76 | 68.30 | 0.0735 | 2.0036 |  |
| Wheat straw | 3.13 | 19.60 | 0.19 | 0.50 | 75.80 | 0.1330 | 2.0031 |  |
| Corn stalks | 7.12 | 26.10 | 0.30 | 1.33 | 64.20 | 0.0125 | 2.0040 |  |
| Corn stalks | 5.08 | 23.00 | 0.25 | 0.87 | 69.70 | 0.0248 | 2.0038 |  |
| Corn stalks | 4.42 | 14.60 | 0.14 | 0.67 | 78.60 | 0.0111 | 2.0035 |  |
| Peanut shells | 5.70 | 45.20 | 0.72 | 1.45 | 47.20 | 0.0109 | 2.0045 | [20] |
| Peanut shells | 2.67 | 24.60 | 0.27 | 0.47 | 68.10 | 4.3900 | 2.0044 |  |

Table S2 Performance evaluation parameters of different machine-learning models for PFRs concentration and g-Factor prediction

| Performance evaluation parameters | Model | Train R2 | Test R2 | Train MSE | Test MSE | AUC |
| --- | --- | --- | --- | --- | --- | --- |
| PFRs concentration prediction | XGBoost | 0.9916 | 0.7193 | 0.0041 | 0.1376 | 0.9614 |
|  | Gradient Boosting | 0.9919 | 0.7328 | 0.0040 | 0.1310 | 0.9643 |
|  | SVR | 0.8760 | 0.7786 | 0.0607 | 0.1086 | 0.9886 |
|  | Shallow NN | 0.8788 | 0.7797 | 0.0593 | 0.1080 | 0.9771 |
|  | Random Forest | 0.9186 | 0.7553 | 0.0398 | 0.1200 | 0.9600 |
|  | Ensemble | 0.9683 | 0.7768 | 0.0155 | 0.1095 | 0.9714 |
|  | XGBoost | 0.9949 | 0.6351 | 7.12 × 10-10 | 5.85 × 10-8 | 0.9971 |
|  | Gradient Boosting | 0.9971 | 0.6599 | 4.10 × 10-10 | 5.45 × 10-8 | 0.9883 |
| g-Factor prediction | SVR | 0.9325 | 0.5767 | 9.40 × 10-9 | 6.79 × 10-8 | 0.9868 |
|  | Shallow NN | 0.7005 | 0.7647 | 4.17 × 10-8 | 3.77 × 10-8 | 0.9780 |
|  | Random Forest | 0.9177 | 0.6880 | 1.15 × 10-8 | 5.00 × 10-8 | 0.9956 |
|  | Ensemble | 0.9784 | 0.6573 | 3.01 × 10-9 | 5.49 × 10-8 | 1.0000 |

References

[1]	Chen D, Xu J, Ling P, Fang Z, Ren Q, et al. 2024. Formation and evolution mechanism of persistent free radicals in biochar during biomass pyrolysis: Insights from biochar's element composition and chemical structure. Fuel 357: 129910. http://doi.org/10.1016/j.fuel.2023.129910.

[2]	Baltrenaite-Gediene E, Lomnicki S, Guo C. 2022. Impact of biochar, fertilizers and cultivation type on environmentally persistent free radicals in agricultural soil. Environmental Technology & Innovation 28: 102755. http://doi.org/10.1016/j.eti.2022.102755.

[3]	Hu Y, Zhang B, Guo Q, Wang S, Lu S. 2022. Characterization into environmentally persistent free radicals formed in incineration fly ash and pyrolysis biochar of sewage sludge and biomass. Journal of Cleaner Production 373: 133666. http://doi.org/10.1016/j.jclepro.2022.133666.

[4]	Bao D, Li Z, Tang R, Wan C, Zhang C, et al. 2021. Metal-modified sludge-based biochar enhance catalytic capacity: Characteristics and mechanism. Journal of Environmental Management 284: 112113. http://doi.org/10.1016/j.jenvman.2021.112113

[5]	Bi D, Yin M, Huang F, Zhang J, Yi W. 2023. Evolution and prediction model of environmentally-persistent free radicals in biomass three-component pyrolytic carbon with pyrolysis temperature. Industrial Crops and Products 206: 117643. http://doi.org/10.1016/j.indcrop.2023.117643.

[6]	Gao Y, Gao Y, Li A. 2025. Effect mechanism of H3PO4 on the formation and transformation of persistent free radicals in biochar. Biochar 7: 28. http://doi.org/10.1007/s42773-024-00405-3.

[7]	Cheng Y, Lu K, Chen Z, Li N, Wang M. 2024. Biochar Reduced the Risks of Human Bacterial Pathogens in Soil via Disturbing Quorum Sensing Mediated by Persistent Free Radicals. Environmental Science & Technology 58: 22343–22354. http://doi.org/10.1021/acs.est.4c07668.

[8]	Hu Y, Tong K, Guo Q, Zhang B, Jiao L, et al. 2022. Effect of controlled temperature and biomass addition on the formed environmental persistent free radicals (EPFRs) in sewage sludge-based biochar from pyrolysis treatment. Journal of Analytical and Applied Pyrolysis 162: 105460. http://doi.org/10.1016/j.jaap.2022.105460.

[9]	Huang D, Luo H, Zhang C, Zeng G, Lai C, et al. 2019. Nonnegligible role of biomass types and its compositions on the formation of persistent free radicals in biochar: Insight into the influences on Fenton-like process. Chemical Engineering Journal 361: 353–363. http://doi.org/10.1016/j.cej.2018.12.098.

[10]	Huang Y, Guo X, Ding Z, Chen Y, Hu X. 2020. Environmentally persistent free radicals in biochar derived from Laminaria japonica grown in different habitats. Journal of Analytical and Applied Pyrolysis 151: 104941. http://doi.org/10.1016/j.jaap.2020.104941.

[11]	Wang Y, Gu X, Huang Y, Ding Z, Chen Y, et al. 2022. Insight into biomass feedstock on formation of biochar-bound environmentally persistent free radicals under different pyrolysis temperatures. RSC Advances 12: 19318–19326. http://doi.org/10.1039/d2ra03052g.

[12]	Xuchao Z , Yi C, Die H, Li Z, Lin W, et al. 2019. Neurotoxic effect of environmental persistent free radicals in rice biochar to Caenorhabditis elegans. China Environmental Science 39: 2644–2651.https://link.cnki.net/doi/10.19674/j.cnki.issn1000-6923.2019.0314.

[13]	Yan X, Cao T, Chen H, Wu J, Xu C, et al. 2025. Formation and evolution of environmentally persistent free radicals in charcoal and soot generated from biomass materials. Journal of Hazardous Materials 488: 137523. http://doi.org/10.1016/j.jhazmat.2025.137523.

[14]	Zhao J, Shen G, Shi L, Li H, Lang D, et al. 2022. Real-World Emission Characteristics of Environmentally Persistent Free Radicals in PM2.5 from Residential Solid Fuel Combustion. Environmental Science & Technology 56: 3997–4004. http://doi.org/10.1021/acs.est.1c08449.

[15]	Zhong D, Zhang Y, Wang L, Chen J, Jiang Y, et al. 2018. Mechanistic insights into adsorption and reduction of hexavalent chromium from water using magnetic biochar composite: Key roles of Fe3O4 and persistent free radicals. Environmental Pollution 243: 1302–1309. http://doi.org/10.1016/j.envpol.2018.08.093.

[16]	Deng R, Luo H, Huang D, Zhang C. 2020. Biochar-mediated Fenton-like reaction for the degradation of sulfamethazine: Role of environmentally persistent free radicals. Chemosphere 255: 126975. https://doi.org/10.1016/j.chemosphere.2020.126975

[17]	Baltrenaite-Gediene E, Lomnicki S, Ogunmusi O. 2024. Research of the impact of environmentally persistent free radicals on chemical element behaviour in the soil-plant system. Chemosphere 364: 143088 http://doi.org/10.1016/j.chemosphere.2024.143088.

[18]	Bi D, Huang F, Jiang M, He Z, Lin X. 2022. Effect of pyrolysis conditions on environmentally persistent free radicals (EPFRs) in biochar from co-pyrolysis of urea and cellulose. Science of the Total Environment 805: 150339. http://doi.org/10.1016/j.scitotenv.2021.150339.

[19]	Fang G, Zhu C, Dionysiou DD, Gao J, Zhou D. 2015. Mechanism of hydroxyl radical generation from biochar suspensions: Implications to diethyl phthalate degradation. Bioresource Technology 176: 210–217. http://doi.org/10.1016/j.biortech.2014.11.032.

[20]	Zhu Z, Gou Q, Duan W, Chen F, Steinberg CEW, et al. 2025. Biochar-mediated degradation of p-nitrophenol as influenced by species of Fe(III). Biochar 7: 65. http://doi.org/10.1007/s42773-025-00448-0.