Supplementary Information

Polymer type, environmental aging, and DOM compositions collectively control DOM fractionation on microplastics

Xiaoxia Zhang1, Yan Lin1, Mengting Zhao1,2, Meiling Zhu1,3, Tianchi Cao1*, Thilo Hofmann4, and Wei Chen1

1 College of Environmental Science and Engineering, Ministry of Education Key Laboratory of Pollution Processes and Environmental Criteria, Tianjin Key Laboratory of Environmental Remediation and Pollution Control, Nankai University, 38 Tongyan Road, Tianjin 300350, China

2 Sinopec Engineering Incorporation, Beijing 100101, China

3 Department of Environmental Protection, Changchun Gold Research Institute Co., Ltd., Changchun130000, China

4 Department of Environmental Geosciences, Centre for Microbiology and Environmental Systems Science, University of Vienna, 1090 Vienna, Austria

Number of pages: 12

Number of tables: 4

Number of figures: 5

* Corresponding author: tianchi.cao@nankai.edu.cn

Text S1. Fluorescence parallel factor (PARAFAC) analysis

Fluorescence excitation–emission matrices (EEMs) were collected using a fluorescence spectrophotometer (F-7100, Hitachi, Japan). Emission spectra were recorded from 280 to 550 nm at 1 nm intervals, while excitation wavelengths were scanned from 220 to 450 nm with 5 nm increments. Both excitation and emission slit widths were set to 5 nm, and the scanning speed was maintained at 12,000 nm min−1. A 290 nm cutoff filter was applied to minimize second-order Rayleigh scattering. Inner-filter effects were corrected using an absorbance-based correction method[1]. PARAFAC modeling was performed in MATLAB R2015b (MathWorks, Natick, MA, USA) using the DOMFluor toolbox (http://www.models.life.ku.dk). The PARAFAC procedure followed established protocols described in previous studies[2–4]. The appropriate number of components was determined based on model residuals, explained variance, and split-half validation to ensure model robustness and component stability. The maximum fluorescence intensity (Fmax) of each PARAFAC component was used as a proxy for its relative abundance. In total, 110 EEM datasets obtained from eight independent adsorption experiments were included in the PARAFAC analysis.

Table S1. Chemical structure of model microplastics (MPs)

| Microplastic | Abbreviation | Chemical structure |
| --- | --- | --- |
| Polyethylene | PE |  |
| Polypropylene | PP |  |
| Polyethylene terephthalate | PET |  |
| Polystyrene | PS |  |
| Polyvinyl chloride | PVC |  |

Table S2. Selected physicochemical properties of pristine, O3-aged, and UV-aged MPs

| MPs a | Molecular weight b |  |  | BET |  |  | Average particle size c (μm) | Total C d (%) | Total O (%) | O/C | H/C | Hydrophobic C (%) | Hydrophilic C (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mn (104 Da) | PDI |  | surface area (m2 g−1) | Micropore volume (10−4 cm3 g−1) | Micropore width (nm) |  |  |  |  |  |  |  |
| PE | 2.28 ± 0.07 | 1.74 |  | 0.26 ± 0.01 | 0.17 ± 0.04 | 1.13 ± 0.06 | 61.2 ± 26.4 | 91.32 | 7.71 | 0.084 | 0.147 | 95.54 | 4.46 |
| PE-O3 | 2.40 ± 0.07 | 1.71 |  | 1.12 ± 0.05 | 0.32 ± 0.06 | 1.13 ± 0.05 | 27.1 ± 19.4 | 84.47 | 14.97 | 0.177 | 0.149 | 82.93 | 17.07 |
| PE-UV | 2.42 ± 0.07 | 1.66 |  | 1.64 ± 0.09 | 0.38 ± 0.09 | 1.13 ± 0.06 | 24.8 ± 19.4 | 91.06 | 8.08 | 0.089 | 0.153 | 91.43 | 8.57 |
| PP | 2.60 ± 0.08 | 1.68 |  | 0.65 ± 0.01 | 0.55 ± 0.11 | 1.10 ± 0.07 | 131 ± 45.1 | 98.70 | 2.30 | 0.000 | 0.149 | 95.17 | 4.83 |
| PP-O3 | 2.41 ± 0.07 | 1.75 |  | 0.85 ± 0.03 | 0.81 ± 0.10 | 1.12 ± 0.06 | 78.4 ± 19.4 | 90.85 | 8.21 | 0.090 | 0.151 | 66.54 | 33.46 |
| PP-UV | 2.17 ± 0.07 | 1.75 |  | 1.47 ± 0.07 | 1.44 ± 0.09 | 1.13 ± 0.06 | 101 ± 42 | 97.76 | 1.46 | 0.015 | 0.153 | 78.74 | 21.26 |
| PET | 2.74 ± 0.08 | 1.97 |  | 0.93 ± 0.03 | 0.59 ± 0.10 | 1.13± 0.06 | 24.7 ± 7.2 | 69.16 | 30.33 | 0.438 | 0.054 | 64.40 | 35.60 |
| PET-O3 | 2.29 ± 0.07 | 2.23 |  | 0.66 ± 0.01 | 1.23 ± 0.17 | 1.11 ± 0.07 | 23.0 ± 7.8 | 70.25 | 29.16 | 0.415 | 0.066 | 51.55 | 48.45 |
| PET-UV | 2.74 ± 0.08 | 2.01 |  | 0.56 ± 0.01 | 0.75 ± 0.11 | 1.12 ± 0.06 | 25.3 ± 8.0 | 69.11 | 30.23 | 0.437 | 0.064 | 59.83 | 40.17 |
| PS | 7.36 ± 0.22 | 2.63 |  | 0.58 ± 0.01 | 1.02 ± 0.11 | 1.12± 0.07 | 108 ± 36 | 100.0 | 0.00 | 0.000 | 0.070 | 96.29 | 3.71 |
| PS-O3 | 6.88 ± 0.20 | 2.73 |  | 0.57 ± 0.01 | 0.60 ± 0.08 | 1.12 ± 0.06 | 132 ± 33 | 59.12 | 38.63 | 0.653 | 0.078 | 75.69 | 24.31 |
| PS-UV | 6.18 ± 0.18 | 3.17 |  | 0.86 ± 0.01 | 1.43 ± 0.19 | 1.11 ± 0.07 | 135 ± 28 | 75.23 | 21.37 | 0.284 | 0.078 | 77.66 | 22.34 |
| PVC | 7.84 ± 0.23 | 2.09 |  | 4.71 ± 0.05 | 7.22 ± 1.10 | 1.06 ± 0.07 | 0.764 ± 0.308 | 71.81 | 1.91d | 0.027 | 0.122 | 82.50 | 17.50 |
| PVC-O3 | 2.96 ± 0.09 | 1.95 |  | 4.75 ± 0.02 | 8.37 ± 1.43 | 1.03 ± 0.09 | 0.667 ± 0.293 | 71.57 | 5.23 | 0.073 | 0.116 | 63.28 | 36.72 |
| PVC-UV | 8.72 ± 0.26 | 1.93 |  | 4.52 ± 0.03 | 7.01 ± 1.10 | 1.06 ± 0.07 | 0.620 ± 0.284 | 70.01 | 4.16 | 0.059 | 0.115 | 74.78 | 25.22 |

a The suffixes “-UV” and “-O3” denote microplastics subjected to UV and ozone aging, respectively. b Mn represents the number-average molecular weight, determined by gel permeation chromatography (GPC). c Surface elemental composition and carbon functional group speciation were analyzed by X-ray photoelectron spectroscopy (XPS). d Surface elemental composition and carbon functional group speciation were analyzed by X-ray photoelectron spectroscopy (XPS).

Table S3. Freundlich isotherm fitting parameters for SRFA and SRHA adsorption on pristine, O3-aged, and UV-aged MPs

| MPs-SRFA | Freundlich model |  |  | MPs-SRHA | Freundlich model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | KF (mg C1−nLn g−1) | n | R2 |  | KF (mg C1−nLn g−1) | n | R2 |
| PE-SRFA | 0.390 ± 0.061 | 0.587 ± 0.072 | 0.958 | PE-SRHA | 0.288 ± 0.022 | 0.824 ± 0.036 | 0.995 |
| PE-O3-SRFA | 1.459 ± 0.080 | 0.175 ± 0.030 | 0.925 | PE-O3-SRHA | 0.232 ± 0.036 | 0.759 ± 0.066 | 0.986 |
| PE-UV-SRFA | 0.878 ± 0.045 | 0.265 ± 0.026 | 0.969 | PE-UV-SRHA | 0.849 ± 0.031 | 0.098 ± 0.019 | 0.887 |
| PP-SRFA | 0.540 ± 0.067 | 0.336 ± 0.057 | 0.925 | PP-SRHA | 0.421 ± 0.053 | 0.184 ± 0.059 | 0.810 |
| PP-O3-SRFA | 0.326 ± 0.062 | 0.573 ± 0.086 | 0.936 | PP-O3-SRHA | 0.510 ± 0.051 | 0.163 ± 0.047 | 0.824 |
| PP-UV-SRFA | 0.222 ± 0.052 | 0.618 ± 0.101 | 0.936 | PP-UV-SRHA | 0.514 ± 0.067 | 0.234 ± 0.064 | 0.806 |
| PET-SRFA | 0.285 ± 0.034 | 0.617 ± 0.052 | 0.981 | PET-SRHA | 0.176 ± 0.035 | 0.879 ± 0.087 | 0.975 |
| PET-O3-SRFA | 0.125 ± 0.008 | 0.835 ± 0.087 | 0.930 | PET-O3-SRHA | 0.222 ± 0.024 | 0.912 ± 0.048 | 0.993 |
| PET-UV-SRFA | 0.264 ± 0.012 | 0.246 ± 0.021 | 0.985 | PET-UV-SRHA | 0.289 ± 0.039 | 0.823 ± 0.062 | 0.986 |
| PS-SRFA | 0.530 ± 0.083 | 0.376 ± 0.074 | 0.889 | PS-SRHA | 0.519 ± 0.136 | 0.639 ± 0.127 | 0.925 |
| PS-O3-SRFA | 0.376 ± 0.061 | 0.336 ± 0.070 | 0.938 | PS-O3-SRHA | 0.537 ± 0.077 | 0.423 ± 0.067 | 0.954 |
| PS-UV-SRFA | 0.882 ± 0.110 | 0.183 ± 0.055 | 0.860 | PS-UV-SRHA | 0.408 ± 0.060 | 0.673 ± 0.070 | 0.973 |
| PVC-SRFA | 0.475 ± 0.026 | 0.437 ± 0.026 | 0.989 | PVC-SRHA | 0.402 ± 0.062 | 0.843 ± 0.075 | 0.986 |
| PVC-O3-SRFA | 0.121 ± 0.027 | 0.540 ± 0.093 | 0.940 | PVC-O3-SRHA | 0.629 ± 0.059 | 0.569 ± 0.047 | 0.980 |
| PVC-UV-SRFA | 0.422 ± 0.009 | 0.102 ± 0.011 | 0.959 | PVC-UV-SRHA | 0.430 ± 0.053 | 0.705 ± 0.060 | 0.982 |

Table S4. Chemical composition of Suwannee River fulvic acid (SRFA) and humic acid (SRHA)

| Type of DOM | Elemental composition (wt%) a |  |  |  |  |  | 13C NMR estimates of carbon distribution a |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C | H | O | N | S |  | Carboxyl | Carbonyl | Aromatic/benzene | Acetal | Heteroatomic aliphatic hydrocarbons | Aliphatic hydrocarbons |
| SRFA | 53.30 | 3.98 | 41.81 | 0.66 | 0.41 |  | 4.2 | 15.6 | 28.9 | 8.1 | 13.3 | 27.4 |
| SRHA | 54.59 | 3.90 | 40.03 | 1.50 | 0.55 |  | 3.9 | 12.8 | 35.3 | 8.9 | 13.4 | 23.9 |

a Elemental composition and 13C NMR data were provided by International Humic Substance Society (IHSS). 13C NMR values represent the percentage distribution of carbon among functional-group classes.

Figure S1. Adsorption of SRFA and SRHA on pristine, O3-aged, and UV-aged MPs. Error bars represent ±1 standard deviation of triplicate measurements (n = 3).

Figure S2. Parity plots and residual error distributions comparing experimentally measured and neural network-predicted distribution coefficients (Kd) for the adsorption of SRFA and SRHA on microplastics. The plot shows a 1:1 line comparison between predicted and real Kd values.

Figure S3. High-resolution X-ray photoelectron spectroscopy (XPS) C 1s spectra of pristine, O3-aged, and UV-aged MPs. Deconvoluted peaks at binding energies of approximately 284.6, 286.6, 287.8, and 288.8 eV are assigned to C–C/C=C (aliphatic or aromatic carbon), C–O (epoxy or hydroxyl), C=O (carbonyl), and O–C=O (carboxyl) functional groups, respectively.

Figure S4. Fourier transform infrared (FTIR) spectra of pristine, O3-aged, and UV-aged MPs. Shaded regions highlight the main oxidation-sensitive bands (including C–O stretching (~1000–1300 cm−1) and C=O stretching (~1700–1750 cm−1)) and C–H stretching (~2950–2850 cm−1).

Figure S5. Percentage change in the DOM distribution coefficient of aged MPs relative to that of pristine MPs (ΔKd%) following O3- and UV-aging for SRFA (a) and SRHA (b). ΔKd % was calculated as [(Kd,aged−Kd,pristine)/Kd,pristine]×100%. Positive values indicate increased adsorption after aging, and negative values indicate decreased adsorption.

References

[1]	Kothawala DN, Murphy KR, Stedmon CA, Weyhenmeyer GA, Tranvik LJ. 2013. Inner filter correction of dissolved organic matter fluorescence. Limnology and Oceanography: Methods 11:616-630. https://doi.org/https://doi.org/10.4319/lom.2013.11.616

[2]	Stedmon CA, Bro R. 2008. Characterizing dissolved organic matter fluorescence with parallel factor analysis: a tutorial. Limnology and Oceanography-Methods 6:572-579. https://doi.org/10.4319/lom.2008.6.572

[3]	Kowalczuk P, Durako MJ, Young H, Kahn AE, Cooper WJ, Gonsior M. 2009. Characterization of dissolved organic matter fluorescence in the South Atlantic Bight with use of PARAFAC model: Interannual variability. Marine Chemistry 113:182-196. https://doi.org/10.1016/j.marchem.2009.01.015

[4]	Nguyen HVM, Lee MH, Hur J, Schlautman MA. 2013. Variations in spectroscopic characteristics and disinfection byproduct formation potentials of dissolved organic matter for two contrasting storm events. Journal of Hydrology 481:132-142. https://doi.org/10.1016/j.jhydrol.2012.12.044