Emerging polymer-based adsorbents for short-chain PFAS: mechanisms, performance and research outlook

Wenjian Yang1, Pengfei Chen1, Jianzhen Huang1, Daoyuan Zu1, Kui Yang2, Xiangtong Kong3, Xiaodong Yang4, Choonsoo Kim5, and Jinxing Ma1,*

- Guangdong Basic Research Center of Excellence for Ecological Security and Green Development, School of Ecology, Environment and Resources, Guangdong University of Technology, Guangzhou 510006, China

- School of Civil and Environmental Engineering, Nanyang Technological University, 50 Nanyang Avenue, Singapore 639798, Singapore

- Department of Applied Biology and Chemical Technology, The Hong Kong Polytechnic University, 999077, Hong Kong Special Administrative Region of China

- China Construction Eighth Engineering Division. Corp. Ltd., Guangzhou 510663, China

- Department of Environmental Engineering with Institute of Energy/Environment Convergence Technologies, Kongju National University, 1223-24, Cheonan-daero, Cheonan-si, 31080, Republic of Korea

Correspondence: Jinxing Ma (jinxing.ma@gdut.edu.cn).

## 1.1 Additional data for the main text

### Supplementary Table S1 Timeline of PFAS regulations and adsorbent development

| Year/Interval | Timeline event | What happened (Summary) | Ref. |
| --- | --- | --- | --- |
| 1938–1945 | Commercial applications: Teflon | Roy J. Plunkett at DuPont discovered PTFE in 1938; later commercialized under the Teflon™ brand. | [1,2] |
| 1956 | Scotchgard | 3M introduced Scotchgard™ fabric protector to the textile market. | [3] |
| 1960s (1966 patent) | AFFF foam | U.S. Naval Research Lab (with 3M) developed PFAS-based aqueous film-forming foams; 1966 patent and rapid adoption. | [4] |
| 2000 | Phase-out of PFOS products | EPA and 3M announced a voluntary phase-out of PFOS-related chemicals and products. | [3,5] |
| ~early 2000s | GAC for PFAS removal | Early studies showed granular activated carbon effectively removes PFOS/PFOA and became a leading drinking-water technology. | [6] |
| ~2008 onward | Cation/Anion Exchange Resins (IX) | Full-scale and column studies demonstrated strong PFAS removal by AER/IX, often complementing GAC. | [7] |
| 2016 | Drinking-water health advisories (70 ng/L) | EPA issued lifetime HAs for PFOA and PFOS (combined 70 ppt) for risk management by states and utilities. | [8] |
| 2017 | β-Cyclodextrin polymer (CDP) | Dichtel group reported β-CD polymer networks that efficiently sequester multiple anionic PFAS from water. | [9] |
| 2016–2018 | Molecularly Imprinted Polymers (MIP) | MIP templated with PFOA/PFOS showed selective removal performance in water. | [10] |
| 2019–2020 | Hydrogels / Ionic fluorogels | Fluorophilic–ionic porous hydrogel resins (“ionic fluorogels”) achieved high selectivity and throughput for mixed PFAS. | [11,12] |
| 2019 | EPA PFAS Action Plan | EPA released the PFAS Action Plan outlining monitoring, treatment, and regulatory pathways. | [13] |
| 2020–2025 | Pretreatment + GAC/IX + high-end membranes/mixed bed | ITRC/EPA guidance recommends source-dependent pretreatment and treatment trains (e.g., GAC/IX with NF/RO) for robust removal and cost control. | [14,15] |
| 2020–2025 | Conductive/redox polymers | Emerging electrochemical systems (e.g., redox-electrodialysis, electro-adsorption) target ultra-short to long-chain PFAS. | [16] |
| 2022 | Updated health advisories for four PFAS | EPA issued extremely low interim HAs for PFOA/PFOS (0.004/0.02 ppt) and final HAs for GenX/PFBS (10/2000 ppt). | [8] |
| 2023 | Proposed NPDWR (six PFAS) | EPA proposed national primary drinking-water rule: MCLs of 4 ppt for PFOA/PFOS; hazard-index approach for PFNA, PFHxS, GenX, PFBS. | [17] |

### Supplementary Table S2 Comparison of PFOA adsorption performance in the reported literature (n = x)

| Adsorbent |  | C0 (mM) | qm(mmol g−1) | teq (h) | qdym(mmol g−1 h−1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Carbon | GAC | 0.12 | 0.39 | 144 | 2.7×10−1 | Yu et al.[18] |
|  |  | 0.29 | 1 | 36 | 2.7×10−2 | Du et al.[19] |
|  | PAC | 0.12 | 0.67 | 2 | 0.34 | Yu et al.[18] |
|  |  | 1.69 | 1.17 | 3 | 0.39 | Li et al.[20] |
|  | CNT | 0.2 | 0.006 | 8 | 8.1×10−4 | Li et al.[21] |
|  |  | 0.12 | 0.32 | 10 | 3.2×10−2 | Li et al.[22] |
| β-CD | Crosslinked β-CD | 0.03 | 0.082 | 13.5 | 6×10−3 | Xiao et al.[23] |
|  | TFH-β-CD | 2.41 | 0.24 | 0.5 | 0.48 | klemes et al[24] |
|  | NH2-β-CD | 0.48 | 1.1 | 48 | 2.3×10−2 | Yang et al[25] |
|  | β-CD-MIP | 1.2 | 2.6 | 3 | 0.86 | Karoyo et al[26] |
|  | Porous β-CD | 2.41 | 0.002 | 48 | 5.1×10−5 | Wang et al[27] |
| MIP | Binary functional MIP | 0.014 | 0.015 | 30 | 5.0×10−4 | Cao et al.[28] |
|  | CMS-MIP | 0.08 | 0.19 | 1 | 0.19 | Guo et al.[29] |
| Hydrogel | fluorinated hydrogels | 0.09 | 0.23 | 5 | 0.046 | Huang et al. [30] |
|  | NH2-PEGDA | 0.25 | 0.11 | 6 | 0.009 | Huang et al.[31] |
|  | F-PEGDA | 0.25 | 0.02 | 6 | 0.001 | Huang et al.[31] |
|  | F and NH2-PEGDA | 0.25 | 0.11 | 6 | 0.009 | Huang et al.[31] |
|  | carbon hydrogel | 2.4×10−4 | 4.6×10−4 | 24 | 1.9×10−5 | Klaus et al. [32] |
| Redox polymers | P(TMPMA-co-TMA) | 0.86 | 2.34 | 5 | 0.47 | Kim et al[33] |
|  | PFMMA | 0.42 | 0.84 | 5 | 0.17 | Medina[34] |
|  | PFPMAm |  | 0.76 |  | 0.15 |  |
|  | PVF |  | 0.56 |  | 0.11 |  |
|  | PFcMA |  | 0.2 |  | 0.04 |  |
|  | PMAECoPF6 |  | 0.65 |  | 0.13 |  |
|  | P(TMPMA-co-TMA)-g-CNT | 0.14 | 1.75 | 4 | 0.43 | Yang et al. [35] |

In this table, C0 refers to the initial concentration (mM); qm refers to the maximum adsorption amount (mmol g−1); teq refers to the equilibrium time (h); qdyn refers to the dynamic adsorption capacity (mmol g−1 h−1); qdyn = qm/teq; GAC refers to the granular activated carbon; PAC refers to the powdered activated carbon; CNT refers to the carbon nanotubes.

Supplementary Table S3 Comparison of Gen X adsorption performance in the reported literature (n = x)

| Adsorbent |  | C0 (mM) | qm (mmol g−1) | teq (h) | qdym (mmol g−1 h−1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Carbonaceous sorbents | GAC | 6.1×10−4 | 3.27×10−3 | 12 | 2.72×10−4 | Tan et al.[36] |
|  |  | 0.152 | 0.79 | 20 | 0.04 | Wang et al.[37] |
|  | PAC | 6.1×10−4 | 4.57×10−3 | 1 | 4.57×10−3 | Tan et al.[36] |
|  |  | 0.152 | 0.79 | 20 | 0.04 | Wang et al.[37] |
| β-CD | Crosslinked β-CD | 3×10−3 | 0.015 | 2 | 7.5×10−3 | Yang et al.[25] |
|  | NH2-β-CD | 0.66 | 0.73 | 2 | 0.37 |  |
| Hydrogel | Ionic fluorogels | 0.144 | 0.8 | 21 | 0.038 | Kumarasamy et al. [38] |
|  | Ionic fluorogels | 0.144 | 0.81 | 21 | 0.038 | Manning [39] |
|  | NH2-PEGDA | 0.183 | 0.087 | 6 | 0.0145 | Huang et al.[31] |
|  | F and NH2-PEGDA | 0.183 | 0.099 | 6 | 0.0165 | Huang et al.[31] |
| Redox polymers | P(TMPMA-co-TMA) | 0.75 | 1.43 | 0.5 | 2.86 | Medina et al.[40] |

In this table, C0 refers to the initial concentration (mM); qm refers to the maximum adsorption amount (mmol g−1); teq refers to the equilibrium time (h); qdyn refers to the dynamic adsorption capacity (mmol g−1 h−1); qdyn = qm/teq; GAC refers to the granular activated carbon; PAC refers to the powdered activated carbon; CNT refers to the carbon nanotube

Supplementary Table S4 Comparison of short-chain PFAS adsorption performance in the reported literature (n = x)

| Adsorbent |  | C0 (mM) | PFAS (C num.) | Removal (%) | teq (h) | Basic quality characteristics of water | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Carbonaceous sorbents | CNT | 1.6×10−6 | PFBA (C4) | 80 | N.A. | pH = 7.1; COD = 5.24 mg L−1; DOC = 1.82 mg L−1; TN = 1.56 mg L−1 (drinking water plant water) | Shi et al.[41] |
|  |  | 1.2×10−6 | PFBS (C4) | 80 | N.A. |  |  |
|  |  | 1.1×10−6 | PFHxA (C4) | 90 | N.A. |  |  |
|  |  | 9.6×10−7 | PFHxS (C6) | 90 | N.A. |  |  |
| β-CD | COFs-β-CD | 5.9×10−6 | PFBS (C4) | 37 | 2 | TOC = 38.6 mg L−1; Cl− = 850 mg L−1; SO42− = 10100 mg L−1; Na+ = 5740 mg L−1; Ca2+ = 0.765 mg L−1; Total Cr = 0.755 mg L−1 (chrome plating wastewater) | Wang et al.[42] |
|  |  | 2.3×10−5 | PFHxS (C6) | 55 | 2 |  |  |
| Hydrogel | Ionic fluorogels | 5.1×10−7 | PFHxA (C6) | 40 | 48 | TOC = 3.4 mg L−1; Cl− = 56.47 mg L−1; SO42− = 101.10 mg L−1; NO3− = 4.23 mg L−1; Na+ = 50.33 mg L−1; Ca2+ = 36.61 mg L−1; Mg2+ = 8.9 mg L−1 (tap water) | Huang et al.[30] |
|  |  |  | PFHxA (C6) | 55 | 48 |  |  |
|  | Ionic fluorogels | 4.6×10−6 | PFBA (C4) | 60 | 2 | pH = 6.2; TOC = 1.3 mg L−1 (treatment plan effluent water) | Kumarasamyet al.[38] |
|  |  | 3.8×10−6 | PFPeA (C5) | 87 | 2 |  |  |
|  |  | 3.2×10−6 | PFHxA (C6) | 90 | 2 |  |  |
|  | Ionic fluorogels | 4.7×10−6 | PFBA (C4) | 58 | 24 | pH = 5.34; TOC ≤ 0.5 mg L−1; conductivity = 180 uS cm−1 (filtered settled conventional water) | Manning et al. [39] |
|  |  | 3.8×10−6 | PFPeA(C5) | 85 | 24 |  |  |
|  |  | 3.8×10−6 | PFHxA (C6) | 90 | 24 |  |  |
| Redox polymers | P(TMA-co-TMPMA-co-METAC) | 0.01 | PFPrA (C3) | 84 | 24 | Cl− = 16.85 mM; SO42− = 6.82 mM; NO3− = 1.75 mM; HPO42− = 0.965 mM (secondary wastewater) | Kim et al.[43] |
|  |  | 0.01 | TFA (C2) | 82 | 24 |  |  |
|  | P(TMPMA-co-TMA) | 3×10−5 | PFHxA (C6) | 70 | 6 | CBOD = 5.0 mg L−1; TSS− = 6.82 mg L−1; NO3−-N = 13 mg L−1; Phos-P = 0.6 mg L−1 (secondary wastewater) | Santiago et al.[44] |

In this table, TOC, total organic carbon; DOC, dissolved organic carbon; COD, chemical oxygen demand; TN, total nitrogen; CBOD, carbonaceous biochemical oxygen demand; TSS, total suspended solids;

2 LCA data

2.1 Synthesis of the polymer

Firstly, 2,2,6,6-tetramethylpiperidin-4-ylmethacrylate (TMPMA, 4.69 g, 20.82 mmol), and 2,2'-Azobis(2-methylpropionitrile) (AIBN, 51.18 mg, 0.31 mmol) were dissolved in 1,4-Dioxane (50 mL) within a 250 mL of Schlenk flask. Then, the solution was degassed by the freeze-pump-thaw method for three cycles and sonicated for 30 minutes to disperse the solute evenly. Subsequently, the solution was heated at 65°C for 20 hours under N2 flow. The resulting substance was precipitated in hexane (300 mL) and centrifugated at 10,000 rpm for 30 min.

Electroactive polymers P(TMPMA-co-TMA) were synthesized via partial oxidation of PTMPMA to poly(4-methacryloyloxy-2,2,6,6-tetramethylpiperidin-1-oxyl) (PTMA) by using Hydrogen peroxide (H2O2). PTMPMA (weight of 63.40 mg, 0.28 mmol) was dissolved in THF (30 mL) and cooled in an ice bath, and then a solution of Hydrogen peroxide in THF (15 mL) was added slowly and stirred for 1 h. Finally, P(TMPMA-co-TMA) was obtained after being dried under reduced pressure.

2.2 Substitution of TEMPMA-class monomer

### 2.2.1 Purpose and scope

For life-cycle modeling of the polymerizable hindered-amine monomer, the foreground inventory for commercially referenced TEMPMA-class methacrylates is substituted with an explicitly specified route to 4-(methacryloyloxy)-2,2,6,6-tetramethylpiperidine (abbrev. 4-MO-TMP). The substitution targets the monomer production stage while preserving downstream polymerization and use-phase assumptions.[45] This choice ensures transparent stoichiometry, controllable unit-process boundaries, and consistent data quality for sensitivity analysis in the absence of uniform supplier LCIs for TEMPMA variants. The synthesis of TEMPMA Unit processes (U) included the following processes[46–54]:

(1) U1. Synthesis of 2,2,6,6-tetramethylpiperidin-4-one (TMP).
Overall: 3 CH3COCH3+NH3→C9H17NO+2 H2O. Inputs: acetone, ammonia, base (cat.), solvent (Org-1). Outputs: TMP, aqueous salts, Org-1 losses, process water.

(2) U2. Selective reduction to 4-hydroxy-TMP (4-HO-TMP).
Carbonyl reduction (e.g., NaBH₄ or catalytic hydrogenation) affords a secondary alcohol. Inputs: TMP, reductant or H2 + catalyst, solvent (Prot-1), quench water. Outputs: 4-HO-TMP, inorganic residues (e.g., borates), or spent catalyst, Prot-1 losses.

(3) U3. Preparation of methacryloyl chloride (or use of methacrylic anhydride, scenario S-Anh).
Route A: CH2=C(CH3)COOH+SOCl2→CH2=C(CH3)COCl+SO2↑+HCl↑(cat. DMF, inhibitor present). Inputs: methacrylic acid, thionyl chloride, DMF (cat.), inhibitor (MEHQ), solvent (Org-2). Outputs: methacryloyl chloride (MAC), SO2/HCl off-gas (scrubbed), Org-2 losses. Route B (S-Anh): methacrylic anhydride used directly; no SO2/HCl formation.

(4) U4. O-acylation to 4-(methacryloyloxy)-TMP (4-MO-TMP).

Schotten–Baumann-type esterification of 4-HO-TMP with MAC (or anhydride) under basic conditions (e.g., TEA or pyridine) with an inhibitor present. Inputs: 4-HO-TMP, MAC (or anhydride), base, solvent (Org-3), inhibitor. Outputs: 4-MO-TMP, Base·HCl salt (or carboxylate), aqueous washings, Org-3 losses.

2.3 LCA inventory

Supplementary Table S5 The amount of adsorbent required to treat 1m3 of water

|  | AC | AER | Polymer | Ref. |
| --- | --- | --- | --- | --- |
| Adsorbent (kg) | 0.189 | 1.647 | 0.12 | [30,38,39,41,44,55] |
| PFAS species | PFOA/PFOS | PFOA/PFOS | PFHxA PFBS |  |

Supplementary Table S6 Inventory data of raw materials and energy required for polymer synthesis

| Step | Flow | Flow category | Role | Unit | Min | Max | Notes |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S1 Polymerization | TMPMA | Material | Monomer | g | 170 | 170 | Batch-defining input; equals monomer charge |
|  | AIBN | Material | Initiator | g | 0.9 | 0.9 | N/A. |
|  | 1,4-Dioxane | Material | Solvent | g | 100 | 300 | Specify solvent recovery fraction (e.g., 0.8–0.95) |
|  | Liquid nitrogen (purge/inert) | Utility | Inerting | L | 1 | 1.8 | Optional purge; density-based mass conversion if needed |
|  | Electricity (thermal/hydrothermal) | Energy | Electricity | kWh | 0.6 | 1.2 | Agitation/heating/cooling as applicable |
| S2 Oxidation | Tetrahydrofuran (THF) | Material | Solvent | g | 100 | 162 | Specify solvent recovery fraction (e.g., 0.8–0.95) |
|  | Hydrogen peroxide (H2O2) | Material | Oxidant | g | 5.91 | 33.49 | Assume concentration (e.g., 30 wt%) |

Supplementary Table S7 Midpoint impact categories and related indicators

| Midpoint impact category | Characterization factors | Unit |
| --- | --- | --- |
| Global warming | Global warming potential (GWP) | kg CO2 eq |
| Stratospheric ozone depletion | Ozone depletion potential (ODP) | kg CFC11 eq |
| Ionizing radiation | Ionising radiation potential (IRP) | kBq Co-60 |
| Ozone formation, Human health | Ozone formation potential: humans (HOFP) | kg NOx eq |
| Fine particulate matter formation | Particulate matter formation potential (PMFP) | kg PM2.5 eq |
| Ozone formation, Terrestrial ecosystems | Ozone formation potential: ecosystems (EOFP) | kg NOx eq |
| Terrestrial acidification | Terrestrial acidification potential (TAP) | kg SO2 eq |
| Freshwater eutrophication | Freshwater eutrophication potential (FEP) | kg P eq |
| Marine eutrophication | Marine eutrophication potential (MEP) | kg N eq |
| Terrestrial ecotoxicity | Terrestrial ecotoxicity potential (TETP) | kg 1,4-DCB |
| Freshwater ecotoxicity | Freshwater ecotoxicity potential (FETP) | kg 1,4-DCB |
| Marine ecotoxicity | Marine ecotoxicity potential (METP) | kg 1,4-DCB |
| Human carcinogenic toxicity | Human toxicity potential (HTPc) | kg 1,4-DCB |
| Human non-carcinogenic toxicity | Human toxicity potential (HTPnc) | kg 1,4-DCB |
| Land use | Agricultural land occupation potential (LOP) | m2a crop eq |

References

[1]	Science History I. 2023. Roy J. Plunkett (1910–1994) and the Discovery of Teflon. https://www.sciencehistory.org/education/scientific-biographies/roy-j-plunkett/

[2]	Chemours. 2024. How Was Teflon™ Discovered? https://www.teflon.com/en/news/how-was-teflon-discovered

[3]	M. 2024. 3M Company Timeline: Scotchgard™ Brand Introduced. https://www.3m.com/3M/en_US/our-company-us/about-3m/history-timeline/

[4]	Laboratory USNR. 2006. NRL Review 2006 (Fire Research / Aqueous Film-Forming Foam (AFFF) advancements)

[5]	Agency USEP. 2000. EPA and 3M Announce Phase Out of PFOS. https://www.epa.gov/archive/epapages/newsroom_archive/newsreleases/33aa946e6cb11f35852568e1005246b4.html

[6]	Ochoa-Herrera V, Sierra-Alvarez R. 2008. Removal of perfluorinated surfactants by sorption onto granular activated carbon, zeolite and sludge. Chemosphere 72:1588-1593. https://doi.org/10.1016/j.chemosphere.2008.04.029

[7]	Higgins CP, Strathmann TJ. 2021. Anion exchange treatment of PFAS in water: A review on history, efficiency, and mechanisms. Water Research

[8]	Agency USEP. 2016. PFOA & PFOS Drinking Water Health Advisories (Fact Sheet)

[9]	Xiao L, Ling Y, Alsbaiee A, Li C, Helbling DE, Dichtel WR. 2017. β-Cyclodextrin Polymer Network Sequesters Perfluorinated Compounds from Water. Journal of the American Chemical Society 139:7689.

[10]	Cao F, Wang L, Ren X, Sun H. 2016. Synthesis of a perfluorooctanoic acid molecularly imprinted polymer for the selective removal of perfluorooctanoic acid in an aqueous environment. Journal of Applied Polymer Science 133. https://doi.org/10.1002/app.43192

[11]	Xiao L, Ching C, Clifford B, Powell C, Michels D, et al. 2020. Ionic Fluorogels for Remediation of Per- and Polyfluorinated Alkyl Substances from Water. ACS Central Science

[12]	Xiao L, Bahl A, Patel A, Jamieson A, Leibfarth FA. 2022. Hydrolytically Stable Ionic Fluorogels for PFAS Remediation and Destruction. Angewandte Chemie International Edition

[13]	Agency USEP. 2019. EPA’s Per- and Polyfluoroalkyl Substances (PFAS) Action Plan

[14]	Agency USEP. 2018. Reducing PFAS in Drinking Water with Treatment Technologies. https://www.epa.gov/sciencematters/reducing-pfas-drinking-water-treatment-technologies

[15]	Yang Z, Zhu Y, Tan X, Gunjal SJJ, Dewapriya P, et al. 2024. Fluoropolymer sorbent for efficient and selective capturing of per- and polyfluorinated compounds. Nature Communications 15https://doi.org/10.1038/s41467-024-52690-y

[16]	Xie M, et al. 2024. Redox-electrodialysis for separation of PFAS from water. Nature Communications

[17]	Interstate T, Regulatory Council PT. 2023. PFAS Technical and Regulatory Guidance Document (Online)

[18]	Yu Q, Zhang R, Deng S, Huang J, Yu G. 2009. Sorption of perfluorooctane sulfonate and perfluorooctanoate on activated carbons and resin: Kinetic and isotherm study. Water Research 43:1150-1158. https://doi.org/10.1016/j.watres.2008.12.001

[19]	Du Z, Deng S, Chen Y, Wang B, Huang J, et al. 2015. Removal of perfluorinated carboxylates from washing wastewater of perfluorooctanesulfonyl fluoride using activated carbons and resins. Journal of Hazardous Materials 286:136-143. https://doi.org/10.1016/j.jhazmat.2014.12.037

[20]	Li J, Li Q, Li L-s, Xu L. 2017. Removal of perfluorooctanoic acid from water with economical mesoporous melamine-formaldehyde resin microsphere. Chemical Engineering Journal 320:501-509. https://doi.org/10.1016/j.cej.2017.03.073

[21]	Li C, Schaffer A, Sequaris JM, Laszlo K, Toth A, et al. 2012. Surface-associated metal catalyst enhances the sorption of perfluorooctanoic acid to multi-walled carbon nanotubes. Journal of Colloid and Interface Science 377:342-346. https://doi.org/10.1016/j.jcis.2012.03.038

[22]	Li Z, Wang L, Li Y, Feng Y, Feng W. 2019. Carbon-based functional nanomaterials: Preparation, properties and applications. Composites Science and Technology 179:10-40. https://doi.org/10.1016/j.compscitech.2019.04.028

[23]	Xiao L, Ling Y, Alsbaiee A, Li C, Helbling DE, Dichtel WR. 2017. beta-Cyclodextrin Polymer Network Sequesters Perfluorooctanoic Acid at Environmentally Relevant Concentrations. Journal of the American Chemical Society 139:7689-7692. https://doi.org/10.1021/jacs.7b02381

[24]	Klemes MJ, Ling Y, Ching C, Wu C, Xiao L, et al. 2019. Reduction of a Tetrafluoroterephthalonitrile-beta-Cyclodextrin Polymer to Remove Anionic Micropollutants and Perfluorinated Alkyl Substances from Water. Angewandte Chemie International Edition 58:12049-12053. https://doi.org/10.1002/anie.201905142

[25]	Yang A, Ching C, Easler M, Helbling DE, Dichtel WR. 2020. Cyclodextrin Polymers with Nitrogen-Containing Tripodal Crosslinkers for Efficient PFAS Adsorption. ACS Materials Letters 2:1240-1245. https://doi.org/10.1021/acsmaterialslett.0c00240

[26]	Karoyo AH, Wilson LD. 2013. Tunable macromolecular-based materials for the adsorption of perfluorooctanoic and octanoic acid anions. J Colloid Interface Sci 402:196-203. https://doi.org/10.1016/j.jcis.2013.03.065

[27]	Wang R, Lin ZW, Klemes MJ, Ateia M, Trang B, et al. 2022. A Tunable Porous beta-Cyclodextrin Polymer Platform to Understand and Improve Anionic PFAS Removal. ACS Central Science 8:663-669. https://doi.org/10.1021/acscentsci.2c00478

[28]	Cao F, Wang L, Tian Y, Wu F, Deng C, et al. 2017. Synthesis and evaluation of molecularly imprinted polymers with binary functional monomers for the selective removal of perfluorooctanesulfonic acid and perfluorooctanoic acid. Journal of Chromatography A 1516:42-53. https://doi.org/10.1016/j.chroma.2017.08.023

[29]	Guo H, Liu Y, Ma W, Yan L, Li K, Lin S. 2018. Surface molecular imprinting on carbon microspheres for fast and selective adsorption of perfluorooctane sulfonate. Journal of Hazardous Materials 348:29-38. https://doi.org/10.1016/j.jhazmat.2018.01.018

[30]	Huang J, Fu K, Liu H, Zhang J, Luo J. 2025. Unveiling the Differential Intensity of Fluorous Active Sites Toward Selective Polyfluoroalkyl Substance Removal: Insights into Adsorption and Desorption Trade-Offs. Environmental Science & Technology 59:10650-10661. https://doi.org/10.1021/acs.est.5c02960

[31]	Huang P-J, Hwangbo M, Chen Z, Liu Y, Kameoka J, Chu K-H. 2018. Reusable Functionalized Hydrogel Sorbents for Removing Long- and Short-Chain Perfluoroalkyl Acids (PFAAs) and GenX from Aqueous Solution. ACS Omega 3:17447-17455. https://doi.org/10.1021/acsomega.8b02279

[32]	Klaus MVX, Gutierrez AM, Hilt JZ. 2023. Development of Poly(acrylamide)-Based Hydrogel Composites with Powdered Activated Carbon for Controlled Sorption of PFOA and PFOS in Aqueous Systems. Polymers 15https://doi.org/10.3390/polym15224384

[33]	Kim K, Baldaguez Medina P, Elbert J, Kayiwa E, Cusick RD, et al. 2020. Molecular Tuning of Redox‐Copolymers for Selective Electrochemical Remediation. Advanced Functional Materials 30:2004635. https://doi.org/10.1002/adfm.202004635

[34]	Baldaguez Medina P, Ardila Contreras V, Hartmann F, Schmitt D, Klimek A, et al. 2023. Investigating the Electrochemically Driven Capture and Release of Long-Chain PFAS by Redox Metallopolymer Sorbents. ACS Appl Mater Interfaces 15:22112-22122. https://doi.org/10.1021/acsami.3c01670

[35]	Yang W, Lai Y, Yang K, Zhou Y, Duan X, et al. 2024. Interface engineering of laminated redox-copolymers for electrochemical remediation of perfluoroalkyl substances. Chemical Engineering Journal 498https://doi.org/10.1016/j.cej.2024.155741

[36]	Tan HM, Pan CG, Yin C, Yu K. 2023. Toward systematic understanding of adsorptive removal of legacy and emerging per-and polyfluoroalkyl substances (PFASs) by various activated carbons (ACs). Environmental Research 233:116495. https://doi.org/10.1016/j.envres.2023.116495

[37]	Wang W, Maimaiti A, Shi H, Wu R, Wang R, et al. 2019. Adsorption behavior and mechanism of emerging perfluoro-2-propoxypropanoic acid (GenX) on activated carbons and resins. Chemical Engineering Journal 364:132-138. https://doi.org/10.1016/j.cej.2019.01.153

[38]	Kumarasamy E, Manning IM, Collins LB, Coronell O, Leibfarth FA. 2020. Ionic Fluorogels for Remediation of Per- and Polyfluorinated Alkyl Substances from Water. ACS Central Science 6:487-492. https://doi.org/10.1021/acscentsci.9b01224

[39]	Manning IM, Guan Pin Chew N, Macdonald HP, Miller KE, Strynar MJ, et al. 2022. Hydrolytically Stable Ionic Fluorogels for High-Performance Remediation of Per- and Polyfluoroalkyl Substances (PFAS) from Natural Water. Angewandte Chemie International Edition 61:e202208150. https://doi.org/10.1002/anie.202208150

[40]	Baldaguez Medina P, Cotty S, Kim K, Elbert J, Su X. 2021. Emerging investigator series: electrochemically-mediated remediation of GenX using redox-copolymers. Environmental Science: Water Research & Technology 7:2231-2240. https://doi.org/10.1039/d1ew00544h

[41]	Shi Y, Mu H, You J, Han C, Cheng H, et al. 2023. Confined water-encapsulated activated carbon for capturing short-chain perfluoroalkyl and polyfluoroalkyl substances from drinking water. Proc Natl Acad Sci U S A 120:e2219179120. https://doi.org/10.1073/pnas.2219179120

[42]	Wang W, Shao H, Zhou S, Zhu D, Jiang X, et al. 2021. Rapid Removal of Perfluoroalkanesulfonates from Water by beta-Cyclodextrin Covalent Organic Frameworks. ACS Appl Mater Interfaces 13:48700-48708. https://doi.org/10.1021/acsami.1c14043

[43]	Kim N, Elbert J, Shchukina E, Su X. 2024. Integrating redox-electrodialysis and electrosorption for the removal of ultra-short- to long-chain PFAS. Nature Communications 15:8321. https://doi.org/10.1038/s41467-024-52630-w

[44]	Roman Santiago A, Yin S, Elbert J, Lee J, Shukla D, Su X. 2023. Imparting Selective Fluorophilic Interactions in Redox Copolymers for the Electrochemically Mediated Capture of Short-Chain Perfluoroalkyl Substances. Journal of the American Chemical Society 145:9508-9519. https://doi.org/10.1021/jacs.2c10963

[45]	Zu D, Liu J, Wei H, Yang K, Tian H, et al. 2025. Comparative life cycle assessment of Fenton-like systems: Insights into the environmental benefits of reductant-driven strategies. Water Research 279:123489. https://doi.org/10.1016/j.watres.2025.123489

[46]	Tokyo Chemical Industry Co L. 2025. 2,2,6,6-Tetramethyl-4-piperidyl methacrylate (TMPM) – product specifications.

[47]	Tian J, Chen L, Zhang C, Yan X, Li Y. 2014. Continuous synthesis of triacetonamine over sulfonic acid-functionalized mesoporous silicas. RSC Advances 4:17860-17865. https://doi.org/10.1039/C4RA00648H

[48]	Thermo Fisher S. 2024. Methacryloyl chloride Safety Data Sheet.

[49]	ScienceDirect T. 2025. Schotten–Baumann Reaction – overview.

[50]	Sarkar S, Malik P, Rout CK. 2023. Continuous production of 2,2,6,6-tetramethyl-4-piperidinol via catalytic hydrogenation of triacetoneamine. RSC Advances 13:5047-5054. https://doi.org/10.1039/D2RA08306J

[51]	Sahoo J, Panda J, Mandal S, Sahoo G. 2024. Factors Governing Chemoselectivity in Alkanolamines: A Panoramic Overview. European Journal of Organic Chemistry https://doi.org/10.1002/ejoc.202400160

[52]	Merck K. 2025. Methacryloyl chloride, contains MEHQ as stabilizer – product information.

[53]	Kristensen TE, Vestli K, Jakobsen CM, Hansen TV. 2015. Chemoselective O-acylation of alcohols in the presence of amines. Beilstein Journal of Organic Chemistry 11:1364-1395. https://doi.org/10.3762/bjoc.11.151

[54]	Debsharma T, Purwanto NS, Fenimore LM, Mitchell S, Kennedy J, Torkelson JM. 2024. BiTEMPS methacrylate dynamic covalent cross-linker providing rapid reprocessability and extrudability of covalent adaptable networks: high-yield synthesis with strong selectivity for disulfide linkages. Polymer Chemistry 15:2167-2176. https://doi.org/10.1039/D4PY00160E

[55]	Liu F, Pignatello JJ, Sun R, Guan X, Xiao F. 2024. A Comprehensive Review of Novel Adsorbents for Per- and Polyfluoroalkyl Substances in Water. ACS ES&T Water 4:1191-1205. https://doi.org/10.1021/acsestwater.3c00569