Supporting Information

High-Capacity and Selective Adsorption of Uranium by Porous Sodium Alginate Composite Gel Microspheres

Yuzhi Xie1,#, Sai Yang1,#, Huanhuan Dong1,#, Xudong Wu1, Lechang Xu2, Jie Kang3, Xue Jiang1, Wenli Zhou1, Jin Zhang1, Xi Wu1, Jian Zhang1, Tao Chen1,*, Wenkun Zhu1,*

[1] CAEA Innovation Center of Nuclear Environmental Safety Technology, School of National Defense & Nuclear Science and Technology, Southwest University of Science and Technology, Mianyang, Sichuan 621010, China

[2] Beijing Research Institute of Chemical Engineering and Metallurgy, CNNC, Beijing 101149, China

[3] CNNC Lanzhou Uranium Enrichment Co., Ltd., Lanzhou 730065, China

*Corresponding author. E-mail: chent@swust.edu.cn(T. Chen), zhuwenkun@swust.edu.cn(W. Zhu).

Supplementary Fig. S1. Digital photographs of the as-prepared microspheres, (a) SA-Ca microspheres, (b) SA-Cu microspheres, (c) SA-CC microspheres.

Supplementary Fig.S2. Effect of initial uranium concentration on the adsorption performance of SA-based materials at pH 4.5.

Pseudo-first-order model:

The adsorption kinetics of U(VI) on gel microspheres was simulated by pseudo-first-order which were used to describe the physisorption behavior.

linear:                                      (S1)

non-linear:                                        (S2)

Pseudo-second-order model:

The pseudo-second-order presumed that the rate limiting step was essentially chemisorption and the mechanism might involve valence forces by sharing or through the exchange of electrons between adsorbate and adsorbent.

linear:                                           (S3)

non-linear:                                         (S4)

the Elovich model:

The Elovich kinetic model considered that the rate-controlling step is the diffusion of the target ions and it revealed the behaviors of chemisorption.

(S5)

the intra-particle diffusion kinetic model:

The intraparticle diffusion kinetic model assumed that the internal diffusion was a velocity-controlled step and the direction of diffusion is random.

(S6)

the bangham model:

The bangham model often used to describe pore diffusion mechanisms.

(S7)

Supplementary Fig. S3. non-linear Linear kinetic model of pseudo-first-order and pseudo-second-order (C0 = 10 mg/L, m/V = 0.1 g/L, pH = 4.5 and T = 298 K).

Supplementary Fig. S1. Kinetic parameters of uranium (VI) adsorption on SA-Ca, SA-Cu and SA-CC.

| Models | Samples | Parameters |  |  |
| --- | --- | --- | --- | --- |
| Pseudo-first-order model |  | Qe (mg/g) | K1 (min-1) | R2 |
|  | SA-Ca | 85.4 | 0.0238 | 0.946 |
|  | SA-CC | 87.7 | 0.0229 | 0.932 |
|  | SA-Cu | 90.6 | 0.0239 | 0.940 |
| Pseudo-second-order model |  | Qe (mg/g) | K2 (g min-1 mg-1) | R2 |
|  | SA-Ca | 92.6 | 0.0013 | 0.987 |
|  | SA-CC | 97.7 | 0.0012 | 0.990 |
|  | SA-Cu | 99.8 | 0.0013 | 0.982 |
| Elovich |  | a (mg g-1 min) | b (g mg-1) | R2 |
|  | SA-Ca | 38.68 | 0.0102 | 0.944 |
|  | SA-CC | 39.23 | 0.0099 | 0.984 |
|  | SA-Cu | 37.92 | 0.0102 | 0.971 |
| Intra-particle diffusion |  | k1 (mg g-1 min-0.5) | C1 (mg g-1 ) | R2 |
|  | SA-Ca | 4.774 | 1.215 | 0.955 |
|  | SA-CC | 4.846 | 5.783 | 0.980 |
|  | SA-Cu | 4.719 | 5.086 | 0.965 |
|  |  | k2 (mg g-1 min-0.5) | C2 (mg g-1 ) | R2 |
|  | SA-Ca | 0.963 | 61.71 | 0.982 |
|  | SA-CC | 1.055 | 65.56 | 0.991 |
|  | SA-Cu | 1.261 | 57.38 | 0.990 |
| Bangham |  | - | α | R2 |
|  | SA-Ca | - | 0.410 | 0.906 |
|  | SA-CC | - | 0.376 | 0.923 |
|  | SA-Cu | - | 0.365 | 0.929 |

Supplementary Fig. S4. Effect of initial uranium (VI) concentration on adsorption capacity of uranium (VI) on SA-Ca, SA-CC and SA-Cu. (m/V = 0.1 g/L, pH = 4.5 and T = 298 K)

the Langmuir isotherms model:

The Langmuir model assumes that monolayer adsorption takes place on the homogenous surfaces. It is one of the most widely used isotherm in adsorption.

the linear format:                                     (S8)

the nonlinear format:                                     (S9)

the Frendlich isotherms model:

The Freundlich model has been regarded as an empirical equation without physical meaning. In many published papers, the Freundlich isotherm was applied to represent the multilayer adsorption on heterogamous surfaces.

the linear format:                                (S10)

the nonlinear format:                                      (S11)

the Redlich-Peterson isotherms model:

The R-P model is an empirical hybrid model of the Langmuir and Freundlich models, which has been frequently applied in the homogeneous or heterogeneous adsorption processes.

(S12)

the Dubinin-Radushkevich isotherms model:

The D–R isotherm model was based on the adsorption potential theory and assumed that the adsorption process was related to micropore volume filling as opposed to layer-by-layer adsorption on pore walls.

(S13)

the Temkin isotherm models:

This Temkin isotherm model takes into consideration the interaction between the adsorbent and the adsorbate in which it ignores the extremely large and low concentration values.

(S14)

Supplementary Fig. S2. Isotherm parameters of uranium (VI) adsorption on SA-Ca, SA-CC and SA-Cu.

| Models | Samples | Parameters |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Langmuir |  | Qm (mg/g) | KL (L/g) | - | R2 |
|  | SA-Ca | 365.7 | 0.327 | - | 0.980 |
|  | SA-CC | 400.8 | 0.562 | - | 0.960 |
|  | SA-Cu | 351.5 | 0.208 | - | 0.993 |
| Freundlich |  | - | KF ((mg/g)(L/mg)n) | nF | R2 |
|  | SA-Ca | - | 165.0 | 4.38 | 0.923 |
|  | SA-CC | - | 103.5 | 3.45 | 0.938 |
|  | SA-Cu | - | 131.4 | 4.01 | 0.868 |
| D-R |  | - | Qd | b | R2 |
|  | SA-Ca | - | 278.3 | 5.97*10-7 | 0.786 |
|  | SA-CC | - | 327.0 | 0.90*10-7 | 0.736 |
|  | SA-Cu | - | 297.7 | 3.02*10-7 | 0.774 |
| R-P |  | KRP (L/g) | α | β | R2 |
|  | SA-Ca | 87.1 | 0.317 | 0.940 | 0.993 |
|  | SA-CC | 397.6 | 1.466 | 0.899 | 0.959 |
|  | SA-Cu | 108.3 | 0.256 | 1.035 | 0.972 |
| Temkin |  | RT | α | β | R2 |
|  | SA-Ca | 0.450 | 8.409 | 0.084 | 0.596 |
|  | SA-CC | 0.391 | 8.865 | 0.020 | 0.479 |
|  | SA-Cu | 0.495 | 3.068 | 0.017 | 0.321 |

Supplementary Fig.S5. Optical and morphological comparison of adsorbent microspheres pre-and post-cycling, (a) The as-synthesized SA-Ca, SA-Cu, and SA-CC microspheres, (b) Microspheres after five adsorption-desorption cycles in a uranium-bearing solution.